DESCRIPTION

OIL UK ANGLO-MAX SUPER LSX 5W-40 is a new generation fully synthetic multigrade engine oil formulated using the latest developments in synthetic technology together with the most up to date advancements in additive chemistry and sets new standards in engine oil performance.

ANGLO-MAX SUPER LSX 5W-40 has been developed to enable outstanding performance to be provided along with full compatibility with emission control after treatment systems. Low SAPS (sulphated ash, phosphorus and sulphur) additive technology allows optimum performance of these systems, including particulate filters, which ensures a high level of continuous pollution control thereby minimising environmental damage.

APPLICATIONS

ANGLO-MAX SUPER LSX 5W-40 is particularly suited to vehicles equipped with anti-pollution systems such as diesel particulate filters where its low SAPS levels will greatly prolong the lifetime of the filter. It is also ideally suited to VW PD (Pumpe Düse) engines as well as modern Vauxhall engines which require the dexos 2 specification.

Typical oil change intervals (Always adhere to vehicle manufacturer’s recommendation)

| CONDITIONS: | SEVERE | DIFFICULT | MODERATE | GOOD |
| --- | --- | --- | --- | --- |
| KMS: | 10,000 | 20,000 | 30,000 | 40,000 |

FEATURES AND BENEFITS

- Effective environmental protection

- Ensures lubricant performance over extended drain intervals

- Effective fuel efficiency

- Very high standards of engine cleanliness

- Exceptional long term anti-wear and oxidation stability

- Excellent high and low temperature performance

- Exceptional long term additive response

PERFORMANCE SPECIFICATIONS

ACEA C3

API SN/CF

MB 229.51

BMW LL-04

VW 502.00/505.01

GM DEXOS 2,

FORD WSS-M2C917-A

RENAULT RN0700/0710

PORSCHE A40

FIAT 9.55535-S2

| TYPICAL PHYSICAL CHARACTERISTICS |
| --- |
| PROPERTY | TYPICAL VALUE |
| Specific Gravity @15.6°C | 0.880 |
| Kinematic Viscosity @ 100°C | 14.20 cSt |
| Kinematic Viscosity @ 40°C | 85.30 cSt |
| Viscosity Index | 169 |
| Pour Point | -38°C |
| Flash Point COC | 225°C |
| TBN (mg KOH/g) | 7.20 |
| Sulphated Ash (% w/w) | 0.78 |