PRODUCT DESCRIPTION

OIL UK ANGLO-MAX SUPER MOTOR OIL 5W-40 is manufactured from fully synthetic base stocks and the latest additive technology available, providing a lubricant with outstanding performance and durability for the most demanding motorist. It offers quicker oil circulation for improved cold starting properties and higher lubricity for reduced internal friction compared with standard mineral based engine oils

APPLICATIONS

ANGLO-MAX SUPER MOTOR OIL 5W-40 is suitable for normally aspirated and turbocharged petrol and diesel engines in passenger cars and light commercials and is suitable for all driving conditions. It is miscible with all synthetic and mineral based engine oils.

FEATURES AND BENEFITS

- Excellent high and low temperature stability

- Effective fuel efficiency

- Very high standards of engine cleanliness

- Exceptional long term anti-wear and oxidation stability

- Exceptional sludge control

- High temperature control prevents ring sticking

PERFORMANCE LEVEL SPECIFICATIONS

ACEA A3/B3, A3/B4

API SL/CF

MB 229.3

BMW Longlife-98

VW 502.00/505.00

RENAULT RN0700/0710

PORSCHE A40

TYPICAL PHYSICAL DATA

| PROPERTY | TYPICAL VALUE |
| --- | --- |
| Specific Gravity @15.6°C | 0.849 |
| Kinematic Viscosity @ 100°C | 14.70 cSt |
| Kinematic Viscosity @ 40°C | 93.00 cSt |
| Viscosity Index | 165 |
| Pour Point | -36°C |
| Flash Point COC | 223°C |
| TBN (mg KOH/g) | 10.20 |