OIL UK ANTIFREEZE LL UNIVERSAL LONG-LIFE ANTIFREEZE

DESCRIPTION

OIL UK ANTIFREEZE LL is an ethylene glycol based engine coolant concentrate, which uses Organic Acid Inhibitor Technology and is free from nitrites, amines, phosphates, borates and silicates. This high quality product is BTC Classification Type 4E. Fleet trials have shown that when used at the correct concentration coolants based on Organic Acid Inhibitor Technology continue to provide effective corrosion protection for up to 250,000 km for passenger cars and 500,000km in commercial vehicles. It is recommended that the coolant is replaced when the above mileages have been reached or after 5 years whichever is the sooner. Unlike traditional coolants which employ inorganic inhibitors, Antifreeze LL has excellent hard water stability and very low inhibitor depletion rates. Antifreeze LL is suitable for all year round usage in automotive and commercial petrol and diesel engines and certain industrial applications.

Product Specification
ASTM D 3306   ASTM D 4985   SAE J 1034   BS 6580: 2010 AFNOR NF R15-601 *  FFV Heft R443   CUNA NC 956-16  UNE 26361 - 88  JIS K 2234 *   NATO S 759   * with the exception of reserve alkalinity

Chrysler MS 9176   Cummins 85T8-2 & 90T8-4 John Deere H 24 B1 & C1   Leyland Trucks LTS 22 AF 10 Mack 014GS 17004   MAN 248, 324 (SNF) & B&W D 36 5600, Mercedes MB 325.3   Renault 41-01-001   VAG TL 774 D/F     Volvo VCS coolant  GM 1899 M, US 6277 M & OPEL GM QL130100  Ford ESE M97B49-A, WSS-M97B44-D & ESD M97B49

APPLICATION

Antifreeze LL is suitable for all year round usage in automotive and commercial petrol and diesel engines and certain industrial applications.

RECOMMENDED DILUTIONS

| Concentration (by volume) | 25% | 33% | 40% | 50% | 60% |
| --- | --- | --- | --- | --- | --- |
| Specific Gravity @ 20°C | 1.030 | 1.045 | 1.060 | 1.074 | 1.087 |
| Freeze Protection (°C)* | -12 | -22 | -27 | -40 | -56 |

*Average of freezing point and pour point.