PRODUCT DESCRIPTION

OIL UK UNIVERSAL ANTIFREEZE is a universal engine antifreeze and coolant, suitable for all year round usage.

Universal Antifreeze is manufactured from pure monoethylene glycol, anti-corrosion additives and inhibitors. It has been specially formulated to be truly universal in its application. It provides a high degree of corrosion protection for all engine cooling systems whether they are predominantly of aluminium or ferrous construction. Universal Antifreeze employs established inhibitor technology. This product is nitrite, amine and phosphate (NAP) free and includes borate and silicate.

APPLICATIONS

Oil UK Universal Antifreeze is suitable for all year round usage in automotive and commercial petrol and heavy duty diesel engines and many industrial applications

FEATURES AND BENEFITS

- Meets and exceeds British Standard BS 6580/2010 specification

- Excellent corrosion protection

- Protects against overheating

- Protects against freezing

- All year round usage

- Suitable for both ferrous and aluminium systems

| Concentration (by volume): | 25% | 33% | 40% | 50% | 60% |
| --- | --- | --- | --- | --- | --- |
| Specific Gravity @ 20°C | 1.03 | 1.045 | 1.06 | 1.074 | 1.087 |
| Freeze Protection (°C) Average of freezing point and pour point | -12 | -22 | -27 | -40 | -56 |

TYPICAL PHYSICAL DATA

| TEST / CHARACTERISTIC | STANDARD |
| --- | --- |
| British Standard | BS 6580: 2010 |
| ASTM | D3306,D4985 |
| SAE | J1034 |
| Freezing Protection Temperature | -40°C |
| Appearance | Clear Blue Liquid |
| Water Content (%w/w) | 4.3 |
| Density @ 15°C (kg/l) | 1.119 |
| Reflux Boiling Point (°C) | 161 |
| pH (50% v/v in deionised water | 7.8 |
| Reserve Alkalinity (ml 0.1N HCl) | 20.5 |

Oil UK Universal Antifreeze contains a bittering agent to prevent accidental consumption.