DESCRIPTION

OIL UK UTTF is a modern Universal Tractor Transmission Fluid for transmissions, hydraulics, final drives and wet brake systems. The very latest agricultural machinery in the modern intensive farming environment needs the protection of a high quality lubricant. Multi-purpose oils are a good compromise but many manufacturers have realised the benefits of using lubricants specifically designed for a given application.

OIL UK UTTF is blended from carefully selected mineral base oils and the very latest in additive technology to produce a specialised lubricant to meet the latest and most severe transmission requirements. It meets the demands of most agricultural transmission specifications and greatly reduces wet brake noise and chatter. It offers outstanding anti wear performance under the most severe conditions.

OIL UK UTTF meets the following performance specifications: API GL-4 John Deere J20C, J20A Massey Ferguson M1145, M1143, M1141, M1135 Case  MAT 3525, MS 1206, MS 1210 New Holland NH 420A, NH 410B Volvo WB101, 97303 Ford ESN-M2C134-D, ESN-M2C86-B ZF TE-ML 03E, 05F, 06K, 17E Kubota UDT Allison C-4 Caterpillar TO-2

APPLICATIONS

OIL UK UTTF is suitable for most modern tractor transmissions, hydraulics, final drives and wet brake systems.

OIL UK UTTF is available either undyed or dyed red for easy identification.

FEATURES AND BENEFITS

- Outstanding anti-wear protection

- Meets the very latest OEM requirements

- Helps reduce wet brake noise and chatter

- Excellent low temperature properties

TYPICAL PHYSICAL PROPERTIES

| OIL UK UTTF | Typical |
| --- | --- |
| Appearance | Clear & Bright |
| Colour | Red or Amber |
| Specific gravity @ 15.6°C | 0.883 |
| Kinematic viscosity @ 100°C (cSt) | 9.70 |
| Kinematic viscosity @ 40°C (cSt) | 61.90 |
| Viscosity Index | 141 |
| Flash point COC (°C) | 224 |
| Pour point (°C) | -38 |