OIL UK ANGLO-MAX SUPER LSC 0W-30 SYNTHETIC LOW VISCOSITY MOTOR OIL

DESCRIPTION

OIL UK ANGLO-MAX SUPER LSC 0W-30 is a fully synthetic low ash automotive engine oil which provides fuel economy benefits without compromising engine protection. It is based on high thermal stability base oil and uses a complex combination of high performance additives which provide excellent engine cleanliness, anti-wear protection and outstanding oxidation resistance.

The SAE 0W-30 viscosity grade promotes fast oil circulation even at low start up temperatures and helps reduce internal friction thereby saving fuel and so reducing emissions. Super LSC 0W-30 also demonstrates a high degree of tolerance towards biodiesel contamination which is known to compromise the oxidation resistance of the engine lubricant.

APPLICATION

. Anglo-Max Super LSC 0W-30 is recommended for the latest Blue HDi engines fitted to Peugeot and Citroen models as well as many petrol engines used in modern Peugeots and Citroens. This product is fully compatible with Selective Catalytic Reduction (SCR) systems as well as Diesel Particulate Filters (DPFs).

FEATURES AND BENEFITS

- Exceptional low temperature properties

- Improved performance

- Fuel economy savings

- Peak performance throughout even the longest service intervals

- Unsurpassed levels of engine protection

PERFORMANCE SPECIFICATIONS

| ACEA C2 PSA B71 2312 |  |
| --- | --- |

| TYPICAL PHYSICAL DATA |
| --- |
| Appearance | Clear & Bright |
| Specific Gravity @ 15.6˚C 0.848 | 0.841 |
| Kinematic Viscosity @ 100˚C (cSt) | 9.8 |
| Kinematic Viscosity @ 40˚C (cSt) | 54.50 |
| Viscosity Index | 168 |
| Flash Point (°C) | 230 |
| Pour Point (°C) | -49 |
| Sulphated Ash % Wt | 0.55 |