OIL UK ANGLO-MAX SUPER LSF 0W-30 SYNTHETIC LOW VISCOSITY MOTOR OIL

DESCRIPTION

Anglo-Max Super LSF 0W-30 is the latest new generation fully synthetic low SAPS (sulphated ash, phosphorus and sulphur) Multigrade engine oil formulated using ultra high quality base stocks and sophisticated additive chemistry.

This product has been developed primarily for modern Ford vehicles requiring the WSS-M2C950-A specification. In addition, this product is recommended for applications requiring an ACEA C2, SAE 0W-30 specification making it suitable for a variety of models from manufacturers including Toyota, Honda and Kia.

PERFORMANCE SPECIFICATIONS

ACEA C2

FORD WSS-M2C950-A

FEATURES AND BENEFITS

- Exceptional low temperature properties

- Compatible with after treatment systems

- Long drain formulation

- Very high levels of engine cleanliness

- Fuel economy savings

- Unsurpassed levels of engine protection

- Excellent high and low temperature performance

- Tolerant of biodiesel contamination

| TYPICAL PHYSICAL DATA |
| --- |
| Appearance | Clear & Bright |
| Specific Gravity @ 15.6˚C 0.848 | 0.841 |
| Kinematic Viscosity @ 100˚C (cSt) | 9.3 |
| Kinematic Viscosity @ 40˚C (cSt) | 43.1 |
| Viscosity Index | 203 |
| Flash Point (°C) | 216 |
| Pour Point (°C) | -50 |
| Sulphated Ash % Wt. | 0.79 |