OIL UK ANGLO-MAX SUPER S 5W-40 HIGH PERFORMANCE SYNTHETIC ENGINE OIL

DESCRIPTION

OIL UK ANGLO-MAX SUPER S 5W-40 is manufactured from fully synthetic base stocks and the latest additive technology available, providing a lubricant with outstanding performance and durability for the most demanding motorist. It offers quicker oil circulation for improved cold starting properties and higher lubricity for reduced internal friction compared with standard mineral based engine oils.

APPLICATION

OIL UK ANGLO-MAX SUPER S 5W-40 is suitable for normally aspirated and turbocharged petrol and diesel engines in passenger cars and light commercials and is suitable for all driving conditions. It is miscible with all synthetic and mineral based engine oils.

FEATURES AND BENEFITS

- Excellent high and low temperature stability

- Provides very high engine cleanliness

- Exceptional anti wear characteristics

- High temperature protection against ring sticking

- Reduced oil consumption and emissions

- Excellent sludge control

- Fuel efficient multigrade

PERFORMANCE SPECIFICATIONS

API SN/CF ACEA A3/B3, A3/B4, VW502.00, 505.00, 501.01, MB 229.5, MB 229.3, GM LL-B-025, BMW Longlife-01, Renault RN0700, RN0710 Porsche A40, PSA B71 2296

| TYPICAL PHYSICAL DATA |
| --- |
| Specific Gravity @ 15.6°C | 0.851 |
| Kinematic Viscosity @ 100°C (cSt) | 14.0 |
| Kinematic Viscosity @ 40°C (cSt) | 88.0 |
| Viscosity Index | 163 |
| Flash Point COC (°C) | 220 |
| Pour Point (°C) | -36 |
| TBN (mg KOH / g) | 10.2 |