PRODUCT DESCRIPTION

OIL UK ANGLO-MAX SUPER SZT 5W-30 is a fully synthetic, high performance, fuel economy engine oil meeting the requirements of the Ford WSS-M2C913-B specification.

ANGLO-MAX SUPER SZT 5W-30 is a balanced blend of synthetic base stocks fortified with state of the art additive technology which produces an exceptional engine oil offering fuel economy and low emission performance. ANGLO-MAX SUPER SZT 5W-30 is the ideal choice for engines requiring a low HTHS (high temperature, high shear) SAE 5W-30 viscosity oil.

APPLICATIONS

ANGLO-MAX SUPER SZT 5W-30 is suitable for both normally aspirated and turbocharged petrol and diesel vehicles. It meets the requirements of the Ford WSS-M2C913-B specification and is miscible with all semi synthetic and mineral oil based engine oils.

Super SZT 5W-30 is recommended for use in selected Ford, Jaguar, Land Rover and Volvo models where a WSS-M2C913-B 5W-30 grade is called for.

BENEFITS

- Meets and surpasses the earlier specifications of WSS-M2C912-A1 and 913-A

- Extended drain capability

- Excellent low temperature stability for improved flow rates

- Provides fuel saving benefits

Fully synthetic formulation

PERFORMANCE LEVEL SPECIFICATIONS

| ACEA | A5/B5, A1/B1 |
| --- | --- |
| API | SL/CF |
| Ford | WSS-M2C913-B |
| BMW | Longlife-01 FE |
| Opel | Pass |
| ISLAC | GF-2 |

TYPICAL PHYSICAL DATA

| Test | Units | Test Method | Typical Properties |
| --- | --- | --- | --- |
| Specific Gravity @ 15.6°C |  |  | 0.857 |
| Kinematic Viscosity @ 100°C | cSt | ASTM D445 | 10.8 |
| Kinematic Viscosity @ 40°C | cSt | ASTM D445 | 62.5 |
| Viscosity Index |  | ASTM D2270 | 165 |
| Flash Point (Open) | °C | ASTM D92 | 225 |
| Pour Point | °C |  | -39 |
| Sulphated Ash | % wt |  | 0.5 |
| TBN | mg KOH / g |  | 8.9 |