OIL UK ANGLO-MAX SUPER E5 15W-40 HIGH PERFORMANCE HEAVY DUTY DIESEL ENGINE OIL

DESCRIPTION

OIL UK ANGLO-MAX SUPER XHD E5 15W-40 is a new generation Super High Performance heavy duty diesel engine oil formulated to meet the most severe lubrication requirements demanded by Mercedes Benz, Cummins and Scania. This product is at the forefront of new heavy duty diesel engine oil technology meeting API CH-4/SL/CF, ACEA E5 and VDS-3 quality making it an ideal choice for all trucks and buses used for inter-city or long haul applications.  It is particularly suited for Cummins engines where piston cleanliness, oxidation, wear and emissions are finely controlled.

OIL UK ANGLO-MAX SUPER XHD E5 15W-40has been designed to meet the requirements of Euro 2 and Euro 3 engines, and a further advantage of this grade is that it has a very highly rated petrol specification (API SL) which serves to improve its scope as a truly top flight engine oil.

FEATURES AND BENEFITS

- High level of piston cleanliness

- Minimises the risk of bore polish, engine wear, piston deposits and bearing corrosion

- Enhanced sludge dispersancy

- Extended oil drain capability with no compromise to engine durability

- Meets the requirements of DAF, Iveco and Scania

PERFORMANCE SPECIFICATIONS

ACEA E5, B4,B3,A2, API CH-4/SL , MB 228.3, MAN M3275, CUMMINS 20071/72/76/77, VOLVO VDS-3, MACK EO-M PLUS, RENAULT RVI RLD, GLOBAL DHD-1, MTU TYPE 2

| TYPICAL PHYSICAL DATA |
| --- |
| PROPERTY | UNIT | TEST METHOD | TYPICAL DATA |
| Specific Gravity @ 15.5°C | g/ml | ASTM D4052 | 0.890 |
| Kinematic Viscosity @ 100°C | cSt | ASTM D445 | 13.9 |
| Kinematic Viscosity @ 40°C | cSt | ASTM D445 | 102.7 |
| Viscosity Index |  | ASTM D2270 | 136 |
| CCS@ -15°C mPa.s |  |  | 3400 |
| Noak Volatility |  |  | 11.7 |
| Total Base Number | mg KOH/g | ASTM D2986 | 10.2 |
| Sulphated Ash | % wt |  | 1.31 |