PRODUCT DESCRIPTION

OIL UK ANGLO-MAX SUPER XHD 20W-50 is a High Performance engine oil formulated to meet the severe lubrication requirements demanded by heavy, medium and light duty diesel and gasoline engines.

ANGLO-MAX SUPER XHD 20W-50 is manufactured from a combination of pure base oils and latest generation performance additive systems to providing superior engine protection, excellent engine cleanliness and enhanced oil life under all operating conditions.,

APPLICATIONS

ANGLO-MAX SUPER XHD 20W-50 is suitable for normally aspirated and turbocharged diesel and petrol engines. It may be used in heavy duty commercial vehicles as well as vans and passenger cars. ANGLO-MAX SUPER XHD 20W-50 is also suitable for off-highway construction plant such as earth moving equipment and tractors, and stationary plant such as heavy duty power generators.

FEATURES AND BENEFITS

- Outstanding Protection – ANGLO-MAX SUPER XHD 20w-50 features an exclusive additive system to ensure maximum soot handling, excellent wear protection and extra-long oil life.

- High Performance – ANGLO-MAX SUPER XHD 20w-50 adapts and protects under the full range of pressures and temperatures found in modern engines, including those operating constantly in high ambient temperatures.

- Improved Engine Cleanliness – The latest generation additive system in ANGLO-MAX SUPER XHD 20w-50 delivers improved engine cleanliness and protection against piston deposits.

- Manufacturers Standards - ANGLO-MAX SUPER XHD 20w-50 satisfies and exceeds the most demanding performance standards of major international engine manufacturers and oil and motor vehicle industry specifications.

PERFORMANCE LEVEL SPECIFICATIONS

API: CH-4/ CF, SL/SJ

ACEA: E3, A3/B3, A3/B4

Mercedes Benz: 228.3, 229.1

MAN: M3275

MTU: Type 2

Mack: EO-L

Volvo: VDS-2

Renault: RVI RD

TYPICAL PHYSICAL DATA

| Test | Units | Test Method | Typical Properties |
| --- | --- | --- | --- |
| Appearance |  | Visual | Clear and Bright |
| Specific Gravity @ 15.5°C |  |  | 0.892 |
| Kinematic Viscosity @ 100°C | cSt | ASTM D445 | 20.8 |
| Kinematic Viscosity @ 40°C | cSt | ASTM D445 | 188.9 |
| Viscosity Index |  | ASTM D2270 | 130 |
| Flash Point (Open) | °C | ASTM D92 | 220 |
| Pour Point | °C | ASTM D97 | -29 |
| Total Base Number | mg KOH/g | ASTM D2986 | 10.6 |