PRODUCT DESCRIPTION

OIL UK SUPER RACING OILS are modern ultra-high performance engine oils formulated to meet the increased power and efficiency demanded by modern engine designs. These superb quality lubricants are engineered using 100% specially selected synthetic base oils and highly advanced additive technology to provide ultimate engine and component protection in modern high performance vehicles.

OIL UK SUPER RACING OILS are designed to maximise performance by providing very high levels of thermal and oxidation stability, engine cleanliness and component wear protection even under the most severe driving and stress conditions.

APPLICATIONS

OIL-UK SUPER RACING OILS are suitable for high performance vehicles, including those with turbocharged, supercharged and naturally aspirated engines.

FEATURES AND BENEFITS

- Excellent high and low temperature performance

- Exceptional long term anti-wear characteristics

- Very high standard of engine cleanliness

- Long lasting dispersant performance and corrosion protection

- Excellent sludge control for stop-go city motoring as well as long distances

- High temperature protection against ring sticking

- Reduced oil consumption and lower emissions

- Compatible with all conventional and synthetic engine oils

PERFORMANCE LEVEL SPECIFICATION

SUPER RACING 0W-40: API: SN/CF ACEA: A3/B4, ACEA A3/B3, A3/B4, VW 502.00/505.00,

MB 229.5, BMW Lomglife-01, Renault RN0700/0710, Porsche A40

SUPER RACING 5W-50: API SN/CF, ACEA A3/B3, A3/B4

SUPER RACING 10W-60: API SN/CF, ACEA A3/B3, A3/B4

TYPICAL PHYSICAL DATA

| PROPERTY | TYPICAL VALUE |
| --- | --- |
| OIL UK SUPER RACING OIL GRADE: | 0w-40 | 5w-50 | 10w-60 |
| Density @ 20°C | 0.843 | 0.860 | 0.863 |
| Kinematic Viscosity @ 100°C (cSt) | 13.5 | 17.6 | 22.6 |
| Kinematic Viscosity @ 40°C (cSt) | 74.8 | 105.7 | 153.1 |
| Viscosity Index | 180 | 184 | 176 |
| Cold Cranking Viscosity (cP) | 5950 @ -35°C | 5600 @ -30°C | 5610 @ -25°C |
| Flash Point °C | 215 | 232 | 238 |
| Pour Point °C | -54 | -40 | -39 |
| TBN (mg KOH/g) | 10.2 | 10.2 | 10.2 |