OIL UK GEARLUBE SUPER SD 75W-90 HIGH PERFORMANCE FULLY SYNTHETIC HEAVY DUTY GEAR OIL

PRODUCT DESCRIPTION

OIL UK GEARLUBE SUPER SD 75W-90 is a fully synthetic, heavy duty, multipurpose, long life gear oil which meets or exceeds the requirements of many industry and manufacturers’ specifications.  It is manufactured from highly refined synthetic base stocks combined with a new powerful state of the art additive and a highly shear stable viscosity modifier.

GEARLUBE SUPER SD 75W-90 is a high performance manual gearbox and axle oil and exhibits unsurpassed load carrying capacity, which is essential for shock load, high torque and high speed service operation.

PRODUCT PERFORMANCE SPECIFICATIONS

API GL-4, GL-5, MT-1, NATO 0-226, MAN 341 E3 & Z2, 342 M3, MB 235.8, Mack GO-J Plus

SAE J2360 (PRI GL 0328), Scania STO 1:0, Arvin Meritor 0-76-N, Military MIL-PRF-2105E, DAF: Meets Requirements Volvo 97312, Iveco Extended Drain, ZF TE-ML 02B, 05B, 07A, 08, 12B, 12L, 12N, 16F, 17B, 19C, 21B

PRODUCT APPLICATIONS

OIL UK GEARLUBE SUPER SD 75W-90 is recommended for highly stressed manual gearboxes, heavily loaded axle drives and synchronised or non-synchronised transmissions where an oil meeting the specifications of this grade is called for.  This grade is particularly suitable for use in Scania, DAF, MAN Volvo and Iveco vehicles.

FEATURES AND BENEFITS

- Longer oil drain capability

- Load carrying durability

- Maximum component protection

- High levels of oxidation resistance

- Outstanding thermal stability

- Greater efficiency

| TYPICAL PHYSICAL DATA |
| --- |
| PROPERTY | UNIT | TYPICAL DATA |
| Specific Gravity @ 15.5°C | g/ml | 0.879 |
| Kinematic Viscosity @ 100°C | cSt | 15.1 |
| Kinematic Viscosity @ 40°C | cSt | 115 |
| Viscosity Index |  | 140 |
| Flash Point (COC) | °C | 205 |
| Pour Point | °C | -53 |