PRODUCT DESCRIPTION

OIL UK ANGLO-MAX SUPER UHPD 5W-30 is a fully synthetic, fuel efficient diesel engine oil meeting the latest long drain requirements. This is the ultimate high performance diesel engine oil, formulated from the highest quality synthetic base oils and performance additives to provide superb levels of performance over extended drain interval

APPLICATIONS

Anglo-Max Super UHPD 5W-30 is suitable for normally aspirated and turbocharged highly rated diesel engines in trucks, buses, coaches, plant and industrial equipment. It can be recommended for the majority of applications where 5W-30, 10W-30, 15W-30 or SAE 30 are recommended. It is miscible with all synthetic and mineral based oils.

Typical oil change intervals (Always adhere to vehicle manufacturer’s recommendation)

| CONDITIONS: | SEVERE | DIFFICULT | MODERATE | GOOD | VERY GOOD |
| --- | --- | --- | --- | --- | --- |
| KMS: | 25,000 | 50,000 | 70,000 | 85,000 | 100,000 |

BENEFITS

- Extended drain periods of up to 100,000kms

- High fuel efficiency and savings

- Reduced oil consumption

- Outstanding soot handling properties

- Excellent high and low temperature performance

- Reduced emissions

- Outstanding anti-wear protection

PERFORMANCE LEVEL SPECIFICATIONS

ACEA E4, API CH-4

VOLVO VDS-2

MB 228.5

MAN M3277

MTU TYPE 3,

RENAULT RVI RXD,

DAF HP-2

TYPICAL PHYSICAL DATA

| Test | Units | Test Method | Typical Properties |
| --- | --- | --- | --- |
| Specific Gravity @ 15.5°C | g/ml | ASTM D4052 | 0.855 |
| Kinematic Viscosity @ 100°C | cSt | ASTM D445 | 11.7 |
| Kinematic Viscosity @ 40°C | cSt | ASTM D445 | 70.0 |
| Viscosity Index |  | ASTM D2270 | 163 |
| Flash Point (Open) | °C | ASTM D92 | 220 |
| Pour Point | °C | ASTM D97 | -42 |
| Total Base Number | mg KOH/g | ASTM D2986 | 15.6 |