OIL UK CHAINSAW OILS 100 & 220 HIGH PERFORMANCE HEAVY CHAINSAW OILS

DESCRIPTION

OIL UK CHAINSAW OIL 100 and CHAINSAW OIL 2200 are high viscosity, tacky chainsaw lubricants which have been formulated using highly refined base oils and performance additives, plus special tacky modifiers which help reduce wear on all chainsaw blades.  They have outstanding oxidation resistance and non-fling properties. Specialised additives help reduce wear on chainsaw blades and provide excellent oxidation resistance which prevents the build-up of unwanted deposits.

APPLICATION

OIL UK CHAINSAW OILS 100 and 220 are suitable for all types of pressure fed chainsaws.

| TYPICAL PHYSICAL DATA |
| --- |
| PROPERTY | UNIT | CHAINSAW OIL 100 | CHAINSAW OIL 220 |
| Appearance |  | Amber | Amber |
| ISO Grade |  | 100 | 220 |
| Specific Gravity @ 15.6°C | g/ml | 0.884 | 0.890 |
| Kinematic Viscosity @ 100°C | cSt | 11.02 | 18.71 |
| Kinematic Viscosity @ 40°C | cSt | 97.01 | 214.04 |
| Viscosity Index |  | 98 | 97 |