PRODUCT DESCRIPTION

OIL UK GEARLUBE HD are specially formulated extreme pressure industrial gear oils.  There is a multiplicity of gear units available today, which vary in design, speed, materials, loading characteristics, operating temperatures and method of application. The trend towards gear manufacture has resulted in higher capacity power transmission from smaller more compact units.

Gear units can be divided into the following types:

- Gears on parallel shafts - Spur, helical and herringbone

- Gears on intersecting shafts - Straight and spiral bevel.

- Gears on crossed shafts - Skew, worm and hypoid.

All of these might be lubricated by splash feed, pump feed or oil bath. To meet these varying demands the Gearlube HD range of industrial gear oils have been formulated using high quality solvent refined base oils and extreme pressure additives. They are available in varying viscosities to meet the exact demands of gearbox requirements.

APPLICATIONS

OIL UK GEARLUBE HD Gear Oils are recommended for most types of enclosed gear applications. They are also suitable for chain drives and bearings.

FEATURES AND BENEFITS

- Extreme pressure additives for extended gear life

- Compatible with most types of seal

- Excellent oxidation stability Outstanding anti-wear protection

PERFORMANCE LEVEL SPECIFICATIONS

- US Steel 224

- AGMA 250.04 & 9005-D94

- David Brown S1.53.101

- Cincinnati Milacron P-74 (C-220)

- DIN 51517 Part 3

TYPICAL PHYSICAL DATA

| Characteristic | ISO 68 | ISO 100 | ISO 150 | ISO 220 | ISO 320 | ISO 460 | ISO 680 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Appearance | Dark Amber | Dark Amber | Dark Amber | Dark Amber | Dark Amber | Dark Amber | Dark Amber |
| Specific Gravity @ 15.5°C | 0.880 | 0.885 | 0.888 | 0.892 | 0.895 | 0.905 | 0.915 |
| ISO Grade | 68 | 100 | 150 | 220 | 320 | 460 | 680 |
| Kinematic Viscosity @ 40°C | 68 | 100 | 150 | 220 | 320 | 460 | 680 |
| Kinematic Viscosity @ 100°C | 8.7 | 11.3 | 14.8 | 18.9 | 24.2 | 30.7 | 38.0 |
| Viscosity Index | 98 | 98 | 98 | 98 | 96 | 96 | 92 |
| Flash Point °C | 212 | 228 | 232 | 236 | 248 | 256 | 262 |
| Pour Point °C | -15 | -12 | -12 | -9 | -9 | -9 | -6 |