PRODUCT DESCRIPTION

OIL UK GEARLUBE SY-PAG is a range of polyalkylene glycol (PAG) based synthetic lubricants which provide outstanding load carrying properties and excellent thermal stability. They have been specifically designed to provide excellent corrosion protection and demulsibility characteristics.

APPLICATIONS

OIL UK GEARLUBE SY-PAG Gear Lubricants allow thermally stable operation at temperatures in excess of 200˚C. Typical applications include the lubrication of calendars, piston compressors and bevel, spiral bevel, helical, enclosed spur and worm gear units. They remain homogenous from below their pour point to temperatures in excess of 250˚C. The anticipated service lifetime of each grade is substantially in excess of 10,000 hours at 100˚C. In industrial enclosed gear units the performance allows for extended drain intervals and, in some cases, for operation as a “fill-for-life” lubricant.

FEATURES AND BENEFITS

- Very high levels of wear protection

- Extended oil drain periods

- Excellent load carrying properties

- Outstanding oxidation stability and resistance to thermal breakdown

- Free from mineral oil, sulphur and chlorine

- Free from metal based additives including lead

- High load carrying properties

- Non-staining towards yellow metals

PERFORMANCE LEVEL SPECIFICATIONS

DIN 51517-PART 3 (CLP), DAVID BROWN TYPE G

TYPICAL PHYSICAL DATA

| Characteristic | ISO 150 | ISO 220 | ISO 320 | ISO 460 |
| --- | --- | --- | --- | --- |
| Appearance | Dark Amber | Dark Amber | Dark Amber | Dark Amber |
| Density @ 20°C (D4052) | 0.944 | 1.006 | 1.006 | 1.007 |
| ISO Grade | 150 | 220 | 320 | 460 |
| Kinematic Viscosity @ 40°C | 150 | 237 | 325 | 433 |
| Kinematic Viscosity @ 100°C | 25 | 31.8 | 44.8 | 63.7 |
| Viscosity Index | 195 | 177 | 196 | 220 |
| Flash Point °C | 191 | 225 | 225 | 225 |
| Pour Point °C | -30 | -30 | -30 | -28 |
| Neutralisation Value (mg KOH/g) (IP139) | 0.90 | 1.09 | 1.12 | 1.15 |
| Total Oxidation Products (%) (IP280) | 0.552 | 0.554 | 0.523 | 0.500 |
| Load Carrying Capacity (IP334. A/8.3/90) FZG Failure Load | >13 | >13 | >13 | >13 |
| Timken OK Load (lbs) (ASTM D2782) | 27 | 27 | 35 | 35 |
| Weld Load (kg) (ASTM D2783) | 168 | 175 | 170 | 170 |
| Copper Strip Corrosion 3 hrs @ 100˚C(IP154) | 1b | 1a | 1a | 1a |
| Rust Prevention (IP135) Procedure A Procedure B | Pass Pass | Pass Pass | Pass Pass | Pass Pass |
| Volume of Foam (ml) Sequence 1 Sequence 2 Sequence 3 | nil/nil nil/nil nil/nil | nil/nil nil/nil nil/nil | nil/nil nil/nil nil/nil | 90/nil 20/nil nil/nil |
| Air Release (min. @ 90˚C) (ASTM D3427) | 19 | 17 | 27 | 25 |
| Demulsibility @ 82˚C Emulsion (ml) Free Water (ml) | 3 37 | 3 37 | 3 37 | 3 37 |