PRODUCT DESCRIPTION

OIL-UK WAYLUBE Slideway Oils are specially compounded oils, developed for the lubrication of slides and ways and intended to eliminate the phenomenon of stick-slip in machine tool operation. The special compounding, plus the use of highly refined base oils give OIL-UK WAYLUBE Slideway Oils outstanding stability, extreme oiliness, adhesiveness (except ISO 32) and exceptional load carrying ability. This enables heavy loading and provides excellent metal wetting properties and serves well as rust preventives as well as lubricants.

APPLICATIONS

OIL-UK WAYLUBE Slideway Oils are non-corrosive to both ferrous and non-ferrous metals. The 32 grade is recommended in machine tools incorporating a hydraulic/slideway lubrication system. OIL-UK WAYLUBE Slideway Oil 68 is suited for horizontal slides and light to moderate loads, and the 220 grade is suitable for vertical slides and heavy loads.

OIL-UK WAYLUB Slideway Oils meet the requirements of: Cincinnati Milacron P-53 (ISO VG 32), Cincinnati Milacron P-47 (ISO VG 68) and Cincinnati Milacron P-50 (ISO VG 220)

FEATURES AND BENEFITS

Eliminates stick-slip

Ensures smooth table action even at slow speeds and under heavy workloads

Provide excellent demulsibility characteristics in the presence of water based cutting fluids

No adverse reaction to resin coated surfaces

Very good corrosion inhibitors

TYPICAL PHYSICAL DATA

| ISO Grade | 32 | 68 | 220 |
| --- | --- | --- | --- |
| Density @ 15°C | 870 | 876 | 898 |
| Viscosity @ 40°C (cSt) | 32 | 68 | 220 |
| Viscosity @ 100°C (cSt) | 5.3 | 8.6 | 19.4C |
| Flash Point °C | >220 | >230 | >240 |
| Pour Point °C | <-21 | <-15 | <-18 |