PRODUCT DESCRIPTION

OIL UK VALIANT 4000 is a premium quality, low carbon forming compressor oil. Valiant 4000 has been designed specifically to offer superior properties when compared to other mineral oil based compressor oils. It is manufactured using carefully selected low volatility mineral oils and inhibitors are added to control oxidation, a problem encountered in the high temperature areas of the discharge zones, and anti-wear agents are added to protect all the mechanical parts in a compressor. Valiant 4000 compressor oil is designed for reciprocating and rotary screw compressors. A 4000-hour drain period is typical with this lubricant.

PERFORMANCE SPECIFICATIONS

DIN 51506 VD-L, PNEUROP POT

FEATURES AND BENEFITS

- Excellent oxidation stability

- Low evaporation and carry over

- Excellent moisture separation

- Extended drain periods

- Reduced gum and carbon build-up

Low Pour Point for better low temperature performance

TYPICAL PHYSICAL DATA

| Appearance |  | Clear Amber Liquid |
| --- | --- | --- |
| Specific Gravity @ 15.6°C |  | 0.876 |
| Kinematic Viscosity @ 40°C | cSt | 48.1 |
| Kinematic Viscosity @ 100°C | cSt | 7.0 |
| Pour Point °C |  | -20 |
| Flash Point °C |  | 219 |
| Viscosity Index |  | 102 |