NEW GENERATION ULTRA HIGH PERFORMANCE SOLUBLE METALWORKING FLUID COMBINING OUTSTANDING MACHINING PERFORMANCE WITH ENHANCED HEALTH AND SAFETY

PRODUCT DESCRIPTION

SOLCUT 6000 CF-B has been formulated to cross all performance boundaries. The unique formulation is based on a combination of synthetic base oil and new generation additives working in perfectly balanced synergy to enable neat oil applications such as broaching and gear cutting to be considered for a switch to water soluble technology.

These levels of machining performance would be difficult to achieve in any high quality semi-synthetic product containing substantial levels of chemical extreme pressure additives but SOLCUT 6000 CF-B achieves even higher levels of performance and combines this with improved tool life capabilities, super extended sump life and new levels of operator safety

#### How do we achieve this?

#### SOLCUT 6000 CF-B has a unique formulation that utilises superior new generation synthetic and safer, naturally based constituents to replace the hazardous chemical additives used as performance enhancers in most high performance soluble metalworking fluids. These include boron and formaldehyde (male fertility concerns) and chlorine (increasingly prohibited in Europe and Scandinavia due to potential environmental impacts).

APPLICATIONS

SOLCUT 6000 CF-B is the perfect choice for soluble metalworking fluid users who are looking to combine outstanding machining performance with new levels of operator safety. It can be used in all types of arduous applications on all types of aluminium alloys, including aerospace, as well as Titanium, high tensile and stainless steels and yellow metals.

AVIATION STANDARDS

SOLCUT 6000 CF-B meets key aviation test specifications including Rolls Royce RPS917 / RRP59000, BAC 5008 standards, ASTM F 483 and ASTM F1110

| MATERIAL SUITABILITY AND RECOMMENDED CONCENTRATIONS |
| --- |
| Material Type | Performance Rating | Applications | Recommended Dilution |
| Titanium | XXXXX | Broaching | 8-10% |
| Aluminium | XXXXX | Tapping | 6-10% |
| Aerospace Aluminium Alloys | XXXXX | Milling | 5-7% |
| High Alloy/Stainless Steels | XXXXX | Turning | 5-7% |
| Copper/Brass | XXXX | Reaming | 8-10% |
| Cast Iron | XX | Sawing | 5-8% |
|  |  | Drilling | 7-10% |

| TYPICAL PHYSICAL DATA |
| --- |
| Appearance of Concentrate: | Amber liquid |
| Odour: | Ultra low |
| Emulsion Appearance: | Fine milky white |
| Specific Gravity: | 0.918 |
| pH @ 5%: | 9.8 |
| IP287 Breakpoint, % Vol: | 3.0 |
| IP125 Breakpoint, % Vol: | 2.0 |
| Stack Corrosion Test | 2.0 |
| De-foam in 50p.p.m. water: | Nil after 10 seconds |
| Reichert Performance @ 10%: | Noise Reduction 12m Load Bearing Capacity 1.66Kg/mm2 |
| Refractometer Correction Factor: | 1.25 |
| Copper/Aluminium Stain | 1a / No Stain |

Product Mixing

Oil UK advises the use of automated mixing systems. If mixing manually, always add the concentrate to the water with maximum agitation, if water is added to the concentrate, the emulsions may prove unstable. Avoid mixing with very cold concentrate or water. Check emulsion strength using a calibrated refractometer. Details of where to purchase equipment and how to use it are available from the Oil UK Technical Department.

Product Management:

The working concentration should be carefully controlled and monitored on a daily basis as higher and lower working concentrations have health and safety implications. Machines should be cleaned out regularly. Fluid and particulate contaminants should be kept to a minimum. This is important especially in terms of bacterial control and is in line with the latest advice from government and professional sources. Detailed reference sources are quoted in the MSDS.

Storage:

- Store in a cool, well ventilated area

- Store inside, ideally between 10°C and 30°C

- Store away from direct heat and frost

- Shelf life 12 months from the date of manufacture

### Avoid water collecting on the barrel top