AN ULTIMATE PERFORMANCE CHLORINE-FREE SOLUBLE METALWORKING FLUID DESIGNED FOR MULTIPLE APPLICATIONS

PRODUCT DESCRIPTION

SOLCUT 4000 CF is a high quality, high lubricity, long life, soluble cutting fluid designed to give outstanding performance when machining a wide variety of materials including aerospace aluminium alloys.

SOLCUT 4000 CF provides superb cutting performance and surface finish, especially with multi-tool CNC machines. The formulation derives its performance characteristics from a synergistic blend of high lubricity performance enhancing additives which help to provide the user with a coolant capable of meeting the most demanding requirements in terms of superb surface finish, long coolant life and extended tool life.

SOLCUT 4000 CF produces a highly stable semi-translucent milky emulsion which provides a very clean working environment. The unique formulation also tolerates hard waters whilst being very low foaming in soft waters.  The product also provides excellent corrosion protection and is non-staining to sensitive aluminium alloys.

APPLICATIONS

### SOLCUT 4000 CF offers excellent cutting performance and can be used in all types of arduous manufacturing applications, including heavy duty machining and creep feed grinding. The performance enhancing additives incorporated into the fluid provide outstanding surface finish on all types of Aluminium, including Aerospace alloys, as well as Titanium, Copper, Brass and high tensile, stainless and medium Steels. The unique formulation prevents scum and soap formation associated with more reactive materials.

### SOLCUT 4000 CF has been proven to have outstanding tool life performance when used in the machining of titanium as well as demonstrating superb properties when used in the machining of high tensile steels.

AVIATION STANDARDS

SOLCUT 4000 CF meets key aviation test specifications including Rolls Royce RPS917 / RRP59000, BAC 5008 standards, ASTM F 483 and ASTM F1110

MATERIAL SUITABILITY AND RECOMMENDED CONCENTRATIONS

| Material Type | Performance Rating | Machining Applications | Recommended Concentration |
| --- | --- | --- | --- |
| Titanium | XXXXX | Broaching | 8-10% |
| Aluminium | XXXXX | Tapping | 6-10% |
| Aerospace Aluminium Alloys | XXXXX | Milling | 5-7% |
| High Alloy/Stainless Steels | XXXXX | Turning | 5-7% |
| Copper/Brass | XXXX | Reaming | 8-10% |
| Cast Iron | XX | Sawing | 5-8% |
|  |  | Drilling | 7-10% |

TYPICAL PHYSICAL DATA

| Appearance of Concentrate: | Amber liquid |
| --- | --- |
| Odour: | Sweet |
| Emulsion Appearance: | Fine milky white |
| Specific Gravity: | 0.980 |
| pH @ 5%: | 9.2 |
| IP287 Breakpoint, % Vol: | 2.0 |
| IP125 Breakpoint, % Vol: | 2.0 |
| De-foam in 50p.p.m. water: | Nil after 10 seconds |
| Reichert Performance @ 10%: | Noise Reduction 27m Load Bearing Capacity 1.97Kg/mm2 |
| Refractometer Correction Factor: | 1.05 |
| Copper/Aluminium Stain Test | 1a / No Stain |