PRODUCT DESCRIPTION

Oil UK Dexron III is a multi-purpose automatic transmission fluid for commercial and passenger car gearboxes meeting a very wide range of specifications. The automatic transmission is one of the most complicated mechanisms in modern automotive engineering and consequently requires complex fluids for efficient operation. Dexron III is manufactured from premium synthetic base stocks and high quality solvent refined base oils with specially selected additives and friction modifiers to produce a lubricant with outstanding durability. It demonstrates excellent frictional stability and offers extended fluid life even when under the most severe conditions.

FEATURES AND BENEFITS

- Long oil life

- Suitable for use as a power steering fluid

- Excellent Protection against wear

- Compatible with all elastomers and other sealing materials

- High temperature stability

- Provides ultimate component protection

APPLICATIONS

Dexron III is recommended for automatic transmissions and power steering units in cars, vans, trucks, buses, agricultural and industrial machines where the following specifications are required:

PERFORMANCE SPECIFICATIONS

GM Dexron IIIH, Dexron IIIG Dexron IID, TASA

MAN 339F, 339 V1 & Z1 339 V2 & Z2 Ford Mercon, Voith 55.6335 (G607) Allison C-4, TES-389

Volvo 97341, 97340 Mercedes-Benz 236.10, 236.9, 236.8, 236.7, 236.6, 236.5, 236.1

ZF TE-ML 02F, 03D, 04D, 09, 11A, 11B, 14A, 14B, 16L, 17C Caterpillar TO-2

TYPICAL PHYSICAL DATA

| Appearance | Clear, red liquid |
| --- | --- |
| Specific Gravity @ 15.6°C | 0.882 |
| Kinematic Viscosity @ 100°C (cSt) | 7.91 |
| Flash Point COC (°C) | 205 |
| Pour Point °C | -53 |