HIGH PERFORMANCE CHLORINE FREE SYNTHETIC WATER-MIX GRINDING FLUID

PRODUCT DESCRIPTION

OIL-UK SOL-GRIND S is a very high performance, long service chlorine-free life water- mix synthetic grinding fluid specially designed to provide exceptional bio-stability, very low residues, and ultra-low foam. OIL-UK SOL-GRIND S is an ultra-modern synthetic long-life water-mix grinding fluid with excellent corrosion protection and cleanliness.

OIL-UK SOL-GRIND S exhibits excellent levels of anti-corrosion protection and cleanliness whilst demonstrating good swarf settlement. This product produces a clear, water white emulsion providing excellent work-piece visibility. The anti-corrosion properties of OIL-UK SOL-GRIND S provide protection of both the machine tool and the finished component and minimum residues found around the grinding wheel when using this high quality product.

APPLICATIONS

OIL-UK SOL-GRIND S provides excellent grinding performance in all types of ferrous metals. It is highly bio stable and gives superb surface finish and extended wheel life. It is low foaming in soft water and suitable hard water as high as 500ppm Calcium Carbonate.

FEATURES AND BENEFITS

| High resistance to bacteria attack | Very long sump life |
| --- | --- |
| Ultra-Low foam | Low hazard – operator friendly |
| Enhanced wheel life | Highly stable emulsion |
| Excellent corrosion protection | Transparent emulsion - Excellent visibility |
| Long term emulsion stability | Superb surface finish |

MATERIALS SUITABILITY AND RECOMMENDED CONCENTRATIONS

| Material Type | Performance Rating | Machining Applications | Recommended Concentration |
| --- | --- | --- | --- |
| Titanium | XXXX | Grinding | 3-5% |
| Aluminium | XXX | Grinding | 3-5% |
| Aerospace Aluminium Alloys | XXX | Grinding | 3-5% |
| High Alloy/Stainless Steels | XXXX | Grinding | 3-5% |
| Copper/Brass | XXX | Grinding | 3-5% |
| Cast Iron | XXXX | Grinding | 3-5% |

TYPICAL PHYSICAL PROPERTIES

| Characteristic | Typical Test Value |
| --- | --- |
| Appearance - Concentrate | Yellow / Amber Fluid |
| Specific Gravity - Concentrate | 1.07 |
| Foaming Tendency | Low |
| Appearance - Emulsion | Transparent |
| IP287 Corrosion Break Point % Vol | 2.5% |
| IP125 Corrosion Break Point % Vol | 2.0% |
| Refractometer factor | 2.0 |
| pH @ 5% Emulsion | 9.3 |
| Aluminium Stain Test | No Stain |

Product Mixing:

OIL-UK advise the use of automated mixing systems. If mixing manually, always add the concentrate to the water with maximum agitation, if water is added to the concentrate, the emulsions may prove unstable. Avoid mixing with very cold concentrate or water. Check emulsion strength using a calibrated refractometer. Details of where to purchase equipment and how to use it are available from the OIL-UK Technical Department.

Product Management:

The working concentration should be carefully controlled and monitored on a daily basis as higher and lower working concentrations have health and safety implications. Machines should be cleaned out regularly. Fluid and particulate contaminants should be kept to a minimum. This is important especially in terms of bacterial control and is in line with the latest advice from government and professional sources. Detailed reference sources are quoted in the MSDS.

Storage:

- Store in a cool, well ventilated area

- Store inside, ideally between 10°C and 30°C

- Store away from direct heat and frost

- Shelf life 12 months from the date of manufacture

- Avoid water collecting on the barrel top