OIL UK ANGLO-MAX SUPER LSR 5W-30 HIGH PERFORMANCE LOW SAPS SYNTHETIC ENGINE OIL

DESCRIPTION

OIL UK ANGLO-MAX SUPER LSR 5W-30 is a new generation fully synthetic low SAPS (sulphated ash, phosphorus and sulphur) multigrade engine oil formulated using the latest developments in synthetic technology together with state of the art additive chemistry which sets new standards in engine oil performance.

ANGLO-MAX SUPER LSR 5W-30 has been developed to provide outstanding performance in terms of engine cleanliness and fuel economy benefits, along with effective emission control and full compatibility with emission control after-treatment systems such as diesel particulate filters. Low SAPS additive technology ensures a high level of continuous pollution control thereby minimising environmental damage.

APPLICATION

ANGLO-MAX SUPER LSR 5W-30 complies with Euro IV and Euro V Diesel Engine emission requirements and is suitable for both petrol and heavy duty diesel engines, including those that are turbocharged. In particular this product is formulated for modern Renault vehicles with after treatment systems such as diesel particulate filters.

FEATURES AND BENEFITS

- Effective environmental protection – Low rates of sulphur , ash and phosphorus (Low SAPS)

- Ensures lubricant performance over extended drain intervals  - Increased drain intervals up to 30,000 km

- Enhanced fuel economy as measured by ACEA M111 FE

- Very high standards of engine cleanliness and wear protection

- Exceptional long term anti-wear and oxidation stability

- Excellent high and low temperature performance

- Exceptional long term additive response

INTERNATIONAL PERFORMANCE SPECIFICATIONS

ACEA C4, 	Renault RN0720,	Mercedes Benz MB 226.51

OIL UK ANGLO-MAX SUPER LSR 5W-30 HIGH PERFORMANCE LOW SAPS SYNTHETIC ENGINE OIL

| TYPICAL PHYSICAL DATA – OIL UK ANGLO-MAX SUPER LSR 5W-30 |
| --- |
| Density @ 15°C | 858 |
| Kinematic Viscosity @ 100˚C (cSt) | 12.6 |
| Kinematic Viscosity @ 40˚C (cSt) | 72.5 |
| Viscosity Index | 166 |
| Pour Point (˚C) | -33 |
| Sulphated Ash (% wt) | 0.4 |
| Flash Point COC (˚C) | 240 |
| TBN (mg KOH / g) | 7.5 |
| CCS @ -30°C mPa.s | 6500 |
| MRV @ -35°C mPa.s | 24800 |