OIL UK ANGLO-MAX SUPER V 0W-20 FULLY SYNTHETIC LOW VISCOSITY MOTOR OIL

DESCRIPTION

OIL UK ANGLO-MAX SUPER V 0W-20 is a premium quality fully synthetic engine oil which, as a result of its specialised formulation and low viscosity, provides significant fuel saving benefits to the motorist. ANGLO-MAX SUPER V 0W-20 also possesses exceptional low temperature characteristics meaning that the oil circulates quickly even in the most demanding cold start conditions.

APPLICATION

OIL UK ANGLO-MAX SUPER V 0W-20 is strongly recommended for many of the latest petrol and diesel engines in Volvo cars. In particular, this product can be used where either of the specification set out below is stated by a vehicle manufacturer.

PERFORMANCE SPECIFICATIONS

ACEA C5, Volvo VCC RBS0-2AE

PERFORMANCE SPECIFICATIONS

- Provides significant reductions in fuel consumption

- Superior oxidative stability

- Excellent low temperature fluidity

- High thermal stability

- Outstanding wear protection

- Fully synthetic formulation

| TYPICAL PHYSICAL DATA |
| --- |
| PROPERTY | UNIT | TEST METHOD | TYPICAL DATA |
| Kinematic Viscosity @ 100°C | cSt | ASTM D445 | 9 |
| Kinematic Viscosity @ 40°C | cSt | ASTM D445 | 47 |
| Viscosity Index |  | ASTM D2270 | 176 |
| Flash Point (Open) | °C | ASTM D92 | >200 |
| Pour Point | °C | ASTM D97 | -46 |
| Total Base Number | mg KOH/g | ASTM D2986 | 8 |
| Sulphated Ash | % wt |  | 0.80 |