DESCRIPTION

OIL UK ANGLO-MAX SUPER XHS 0W-40 is manufactured from fully synthetic base stocks and the latest additive technology available, providing a lubricant with outstanding performance and durability for the most demanding motorist. It offers quicker oil circulation for improved cold starting properties and higher lubricity for reduced internal friction compared with standard mineral based engine oils.

APPLICATIONS

OIL UK ANGLO-MAX SUPER XHS 0W-40 is suitable for normally aspirated and turbocharged petrol and diesel engines in passenger cars and light commercials and is suitable for all driving conditions. It is recommended where one of the following specifications is required. It is miscible with all synthetic and mineral based engine oils.

Typical oil change intervals (Always adhere to vehicle manufacturer’s recommendation)

| CONDITIONS: | SEVERE | DIFFICULT | MODERATE | GOOD |
| --- | --- | --- | --- | --- |
| KMS: | 10,000 | 20,000 | 30,000 | 40,000 |

FEATURES AND BENEFITS

- Excellent high and low temperature stability

- Provides very high levels of engine cleanliness

- Exceptional anti wear characteristics

- High temperature protection against ring sticking

- Reduced oil consumption and emissions

- Very low volatility

PERFORMANCE SPECIFICATIONS

API SN/CF, ACEA A3/B3, A3/B4

VW 502.00/505.00, MB 229.5, BMW LONGLIFE-01, RENAULT RN0700/0710, PORSCHE A40

TYPICAL PHYSICAL CHARACTERISTICS

| PROPERTY | UNIT | TEST METHOD | TYPICAL DATA |
| --- | --- | --- | --- |
| Specific Gravity @ 15.5°C | g/ml | ASTM D4052 | 0.843 |
| Kinematic Viscosity @ 100°C | cSt | ASTM D445 | 13.51 |
| Kinematic Viscosity @ 40°C | cSt | ASTM D445 | 74.81 |
| Viscosity Index |  | ASTM D2270 | 180 |
| Flash Point (Open) | °C | ASTM D92 | 223 |
| Pour Point | °C | ASTM D97 | -45 |
| Total Base Number | mg KOH/g | ASTM D2986 | 10.20 |