DESCRIPTION

OIL-UK SUPER MOTOR OIL 5W-30 is a semi-synthetic fuel efficient multigrade engine oil based on ultra-high quality synthetic and mineral base stocks and formulated with the very latest in advanced additive technology.

OIL-UK SUPER MOTOR OIL 5W-30 has been developed to provide high performance through excellent component protection, film strength and oxidation stability.

APPLICATIONS

OIL-UK SUPER MOTOR OIL 5W-30 is suitable for normally aspirated and turbo charged diesel and petrol engines in passenger cars and light commercial modern vehicles. This product is miscible with all synthetic and mineral based engine oils.

Typical oil change intervals (Always adhere to vehicle manufacturer’s recommendation)

| CONDITIONS: | SEVERE | DIFFICULT | MODERATE | GOOD |
| --- | --- | --- | --- | --- |
| KMS: | 7,500 | 15,000 | 20,000 | 30,000 |

FEATURES AND BENEFITS

- Excellent high and low temperature performance

- High quality semi-synthetic formulation

- Suitable for Ford Zetec Engines

- High standard of engine cleanliness

- Long lasting dispersant performance and corrosion protection

- Excellent sludge control for stop-go city motoring as well as long distances

- High temperature protection against ring sticking

- Reduced oil consumption and lower emissions

- Superior performance over standard mineral oil based products

PERFORMANCE SPECIFICATIONS

API: SL/SJ/CF ACEA: A1/B1

Ford: WSS-M2C-912-A1, WSS-M2C-913-A, WSS-M2C-913-B

BMW: LL-01 FE, Opel / Vauxhall: Pass, ILSAC: GF-2

| TYPICAL PHYSICAL CHARACTERISTICS |
| --- |
| Specific Gravity @15.6°C | 0.873 |
| Kinematic Viscosity @ 100°C | 13.9 cSt |
| Kinematic Viscosity @ 40°C | 92.7 cSt |
| Viscosity Index | 155 |
| Pour Point | -32°C |
| Flash Point COC | 226°C |
| TBN (mg KOH/g) | 10.2 |