DESCRIPTION

OIL UK ANGLO-MAX SUPER PLUS 15W-40 is a high performance multigrade engine oil manufactured from highly refined, high viscosity index base oils and carefully balanced additives, producing a superior quality petrol and diesel engine oil.

This product offers excellent high temperature stability and stay in grade performance. The additives used reduce the unwanted gums and varnishes in cylinders, on pistons and in turbochargers.

APPLICATIONS

ANGLO-MAX SUPER PLUS 15W-40 is suitable for normally aspirated and turbo charged diesel engines and petrol engines in passenger cars, light and heavy commercials, buses, agricultural, plant and construction equipment. It is miscible with all synthetic and mineral based engine oils.

Typical oil change intervals (Always adhere to vehicle manufacturer’s recommendation)

| CONDITIONS: | SEVERE | DIFFICULT | MODERATE | GOOD |
| --- | --- | --- | --- | --- |
| KMS: | 7,500 | 15,000 | 30,000 | 30,000 |

FEATURES AND BENEFITS

- Excellent engine protection performance

- Protection against sludge formation

- Stay in grade performance

- Good anti wear properties

PERFORMANCE SPECIFICATIONS

API: SL/CH-4, ACEA: E3, A3/B4, A3/B3

Mercedes MB228.3, 229.1, Volvo VDS-2, Renault RVI RD, MTU Type 2, MAN M3275,

Mack EO-L

| TYPICAL PHYSICAL CHARACTERISTICS |  |
| --- | --- |
| Specific Gravity @ 15.6°C | 0.888 |
| Kinematic Viscosity @ 40°C (cSt) | 106 |
| Kinematic Viscosity @ 100°C (cSt) | 14.6 |
| Viscosity Index | 139 |
| Flash Point COC (°C) | 215 |
| Pour Point (°C) | -29 |
| TBN (mg KOH / g) | 10.65 |