PRODUCT DESCRIPTION

OIL UK HYLOAD FR-E46 is a HFDU type fire resistant hydraulic fluid based on a high purity, synthetic ester and fortified with carefully selected additives to achieve excellent hydraulic fluid performance. It does not contain water, mineral oil or phosphate ester.

APPLICATIONS

HYLOAD FR-E46 is suitable for a wide range of industrial applications where there is a fire risk, where there is environmental sensitivity and/or where extremes of ambient temperatures prevail. HYLOAD FR-E46 can be used wherever an ISO 46 HFDU fluid is called for.

PERFORMANCE LEVELS

- ISO 15380 HEES

- Denison HF-2, HF-6

- Meets the requirements of standards OECD 201, 202 & 203 for Eco toxicity and OECD 301B for biodegradability.

- ISO 6743-4 HFDU

FEATURES AND BENEFITS

- Self-extinguishing properties limit the spread of fire

- Non-toxic, non-irritating and contains no hazardous ingredients

- Readily biodegradable and non-toxic to aquatic life

- Offers equivalent lubrication of premium grade anti-wear hydraulic oils

- High levels of oxidation resistance to prolong fluid life

- Low pour point

- High viscosity index ensures suitability over a wide temperature range

- Compatible with mineral oil and vegetable oil based hydraulic fluids

HOSE COMPATIBILITY

Independent testing has been conducted to the standard ISO 1817 to verify compatibility with two typical types of hose material. Samples of hose material were immersed in Ultramax FRE 46 for 168 hours at 100°C.

TEST RESULTS

| Hose Material | Result | Specification |
| --- | --- | --- |
| NBR Compound-Braided Hose | +2% Swelling | <25% Swelling (EN 857) |
| CR/SBR Compound - Spiralled Hose | +27% Swelling | <60% Swelling (EN 856) |

TYPICAL PHYSICAL DATA

| OIL UK HYLOAD FR-E46 |
| --- |
| Test | Typical Result |
| ISO Viscosity Grade | 46 |
| Appearance | Yellow liquid |
| Specific Gravity @ 20°C | 0.930 |
| Kinematic Viscosity @ 40°C | 46 cSt |
| Kinematic Viscosity @ 100°C | 9.3 cSt |
| Flash Point (COC) °C | 310 |
| Pour Point °C | -45 |
| Viscosity Index | 191 |