DESCRIPTION

OIL UK ANGLO-MAX SUPER GM-S 5W-30 is a new generation fully synthetic multigrade engine oil formulated using the latest developments in synthetic technology together with the most up to date advancements in additive chemistry, and sets new standards in engine oil performance.

ANGLO-MAX SUPER GM-S 5W-30 has been developed to provide excellent performance in all driving conditions, and contains special additives to reduce the low speed pre-ignition and chain wear issues, which can effect some turbo charged and petrol direct injection engines.

APPLICATION

ANGLO-MAX SUPER GM-S 5W-30 is particularly suited to Opel/ Vauxhall/ General Motors models with petrol direct injection engines, but this high performance engine oil is suitable for engines requiring the following performance specifications are stated:

Typical oil change intervals (Always adhere to vehicle manufacturer’s recommendation)

| CONDITIONS: | SEVERE | DIFFICULT | MODERATE | GOOD |
| --- | --- | --- | --- | --- |
| KMS: | 10,000 | 20,000 | 30,000 | 40,000 |

FEATURES AND BENEFITS

( Low Speed Pre-Ignition reduction

( Enhances fuel economy

( Excellent anti-wear protection

( Exceptional piston cleanliness

( Protection against sludge

PERFORMANCE SPECIFICATIONS

API SN Plus, SN, GM dexos1, Gen 2, ILSAC GF-5

| TYPICAL PHYSICAL CHARACTERISTICS |
| --- |
| OIL UK ANGLO-MAX SUPER GM-S 5W-30 | Typical |
| Kinematic Viscosity @ 100°C (cSt) | 11.2 |
| Kinematic Viscosity @ 40°C (cSt) | 65.1 |
| Viscosity Index | 166 |
| Flash Point (Closed) (°C) | 225 |
| TBN (mg KOH/g) | 8.3 |
| Pour Point °C | -42 |
| Specific Gravity @ 15.60°C | 0.847 |