OIL UK HYLOAD BIO PREMIUM BIODEGRADABLE HYDRAULIC OILS RANGE

DESCRIPTION

The OIL UK HYLOAD BIO range are superior biodegradable hydraulic oils manufactured from natural refined rapeseed oil. They are fortified with proprietary additives to provide excellent anti-wear and high temperature performance that is as good as if not better than that found in mineral oil based grades.

HYLOAD BIO oils are completely free of zinc and all other heavy metals thus avoiding environmental pollution through spillage or leakage.

HYLOAD BIO SE 46 is a synthetic ester based, biodegradable hydraulic fluid which offers many advantages over vegetable oil based biodegradable hydraulic fluids. It is far more resistant to oxidation which in turn means a greatly reduced risk of gumming and varnish deposits. As a result, HYLOAD BIO SE 46 provides a service life many times longer than that of conventional biodegradable fluids. Hyload BIO SE 46 also possesses improved low temperature fluidity and contains high quality ash-less performance additives which will provide superior anti-wear protection, corrosion inhibition and low foaming properties.

APPLICATION

The OIL UK HYLOAD BIO range is recommended as a replacement for mineral oil based hydraulic oils, particularly where spillage or loss in plant and equipment used near to, or for the construction of, waterways and reservoirs.   Hyload Bio oils are also recommended for all applications where some contact with humans or animals is a possibility.   These applications include elevators, door openers, aircraft baggage handlers, people movers and total system losses, that frequently occur from burst hoses on hard worked hydraulic equipment.

FEATURES AND BENEFITS: HYLOAD BIO GRADES

- Very high levels of biodegradability

- Incorporates inhibitors for protection against all forms of corrosion

- Good anti-foaming and air release properties

- Good demulsification characteristics

- Excellent anti-wear performance

- High oxidation resistance and thermal stability

- Environmentally friendly

OIL UK HYLOAD BIO PREMIUM BIODEGRADABLE HYDRAULIC OILS RANGE

FEATURES AND BENEFITS: HYLOAD BIO SE 46

- Thermally stable synthetic formulation

- Meets European Ecolabel criteria

- Ash free

- Extended drain intervals

- Low pour point

- Compatible with mineral and vegetable oil based fluids

PERFORMANCE SPECIFICATIONS

HYLOAD BIO GRADES:

- Biodegradability (CEC-L-33-T-82) >98%

- DIN  51524 Part 3 (except D943) ISO 11158 category HV (except D943)

HYLOAD BIO SE 46:

- European Ecolabel

- ISO 15380 HEES

- Swedish Standard SS 15 54 34

- Denison HF-2, HF-6

- Meets the requirements of standards OECD 201, 202 & 203 for ecotoxicity and OECD 301B for biodegradability

TYPICAL PHYSICAL DATA

| HYLOAD BIO ISO VISCOSITY GRADE: | 32 | 46 | 68 | SE 46 |
| --- | --- | --- | --- | --- |
| Specific Gravity @ 15.6°C | 0.923 | 0.925 | 0.926 | 0.966 |
| Kinematic Viscosity @ 40°C (cSt) | 32.0 | 46.0 | 68.0 | 46 |
| Kinematic Viscosity @ 100°C (cSt) | 7.4 | 9.7 | 14.5 | 8.3 |
| Viscosity Index | 209 | 208 | 228 | 157 |
| Flash Point °C | 210 | 220 | 225 | >280 |
| Pour Point °C | -30 | -25 | -24 | <-39 |
| BIODEGRADABILITY | >98% | >98% | >98% | >98% |