OIL UK HYLOAD BIO SYN 46 SYNTHETIC ULTRA-HIGH PERFORMANCE BIODEGRADABLE HYDRAULIC OIL

DESCRIPTION

OIL UK HYLOAD BIO SYN 46 is a synthetic ester based, biodegradable hydraulic fluid which offers many advantages over vegetable oil based biodegradable hydraulic fluids. It is far more resistant to oxidation which in turn means a greatly reduced risk of gumming and varnish deposits.

As a result, HYLOAD BIO SYN 46 provides a service life many times longer than that of conventional biodegradable fluids. It also possesses improved low temperature fluidity and contains high quality ash-less performance additives which will provide superior anti-wear protection, corrosion inhibition and low foaming properties.

APPLICATION

OIL UK HYLOAD BIO SYNTH 46 is recommended as an ultra-high performance replacement for vegetable oil based biodegradable and mineral oil based hydraulic oils, particularly where spillage or loss in plant and equipment used near to, or for the construction of, waterways and reservoirs.

Typical applications include construction equipment, agricultural machinery, forestry, horticultural equipment and mobile plant.

FEATURES AND BENEFITS: HYLOAD BIO GRADES

- Very high thermal stability and biodegradability

- Low pour point for good cold temperature performance

- Good anti-foaming and air release properties

- Good demulsification characteristics

- Excellent anti-wear performance

- High oxidation resistance

- Meets European ecolabel criteria

- Extended oil drain intervals from longer service life

- Ash-Free

- Compatible with mineral and vegetable oil based fluids

OIL UK HYLOAD BIO SYN 46 SYNTHETIC ULTRA-HIGH PERFORMANCE BIODEGRADABLE HYDRAULIC OIL

FEATURES AND BENEFITS: HYLOAD BIO SE 46

- Thermally stable synthetic formulation

- Meets European Ecolabel criteria

- Ash free

- Extended drain intervals

- Low pour point

- Compatible with mineral and vegetable oil based fluids

PERFORMANCE SPECIFICATIONS

- European Ecolabel

- ISO 15380 HEES

- Swedish Standard SS 15 54 34

- Denison HF-2, HF-6

- Meets the requirements of standards OECD 201, 202 & 203 for ecotoxicity and OECD 301B for biodegradability

TYPICAL PHYSICAL DATA

| HYLOAD BIO ISO VISCOSITY GRADE: | Typical Test Result |
| --- | --- |
| Specific Gravity @ 15.6°C | 0.966 |
| Kinematic Viscosity @ 40°C (cSt) | 46.0 |
| Kinematic Viscosity @ 100°C (cSt) | 8.3 |
| Viscosity Index | 157 |
| Flash Point °C (COC) | >280 |
| Pour Point °C | -39 |
| BIODEGRADABILITY (CEC-L-33-T-82) % | >98 |