PRODUCT DESCRIPTION

OIL UK SUPER 20W-50 is a multigrade engine oil manufactured from highly refined, high viscosity index base oils and carefully balanced additives producing a high quality petrol and diesel engine oil. It offers excellent high temperature stability and stay in grade performance. The additives used reduce the unwanted gums and varnishes in cylinders, on pistons and in turbochargers

APPLICATIONS

OIL UK SUPER XHD 20W-50 is suitable for both normally aspirated and turbocharged heavy duty diesel and petrol engines and is an ideal choice for on-highway applications in trucks and buses as well as off-highway applications in the agricultural and construction sectors.

Typical oil change intervals (Always adhere to vehicle manufacturer’s recommendation)

| CONDITIONS: | SEVERE | DIFFICULT | MODERATE | GOOD | VERY GOOD |
| --- | --- | --- | --- | --- | --- |
| KMS: | 7,500 | 15,000 | 20,000 | 30,000 | 40,000 |

- Enhanced component protection

- Excellent engine cleanliness and oxidation control

- Reduced downtime due to unscheduled maintenance

- Excellent performance

PERFORMANCE LEVEL SPECIFICATIONS

API SG/CF-4

Caterpillar TO-2

Mercedes Benz 227.1

MAN 271

Allison C3

US Military MIL-L-2104E

CCMC G3/PD2Volvo VDS-2

VW 505.00

TYPICAL PHYSICAL DATA

| Test | Units | Test Method | Typical Properties |
| --- | --- | --- | --- |
| Appearance |  | Visual | Clear and Bright |
| Specific Gravity @ 15.5°C |  |  | 0.888 |
| Kinematic Viscosity @ 100°C | cSt | ASTM D445 | 20.68 |
| Kinematic Viscosity @ 40°C | cSt | ASTM D445 | 185.04 |
| Viscosity Index |  | ASTM D2270 | 132 |
| Flash Point (Open) | °C | ASTM D92 | 229 |
| Pour Point | °C | ASTM D97 | -30 |
| Total Base Number | mg KOH/g | ASTM D2986 | 9.06 |