PRODUCT DESCRIPTION AND PERFORMANCE SPECIFICATION

OIL UK DOT 4 ESP-VW 265/175 is a high performance; low viscosity Brake Fluid which has been specially formulated to enable Electronic Stability Program (ESP) systems to operate effectively over a wide temperature range. Suitable for all ESP and other conventional brake systems using Glycol Ether based Brake Fluids.

The product shall fully meet the requirements of the latest issue of the US FMVSS 116 DOT 4, DOT 3, SAE J 1703, SAE J 1704 and ISO 4925 (Classes 3, 4 & 6) Specifications. The product shall also meet the requirements of VW standard 50 114 (TL766Z:2006) and the parameters below.

| TYPICAL PHYSICAL CHARACTERISTICS |  |
| --- | --- |

| Test Required |  | Typical Results | Specification |
| --- | --- | --- | --- |
| Dry Equilibrium Reflux Boiling Point, °C | 270 | 265 °C. Min. |
| Wet Equilibrium Reflux Boiling Point, °C | 180 | 175 °C. Min. |
| Kinematic Viscosity | @ -40 °C, cSt | 635 | 700 cSt Max. |
|  | @ 100 °C, cSt | 2.02 | 1.5 cSt Min. |
| pH |  | 7.39 | 7 – 11.5 |
| High Temperature Stability, °C | -1 | +/- 3.0 °C. Max |
| Chemical Stability, °C |  | +1 | +/- 3.0 °C. Max |
| Fluidity & Appearance | @ -40 °C | Pass, 2 seconds | No freezing, Bubble time 3 sec. Max |
|  | @ -50 °C | Pass, 4 seconds | No freezing, Bubble time 5 sec. Max |
| Water Tolerance | @ -40 °C | Clear, 2 seconds | 3 seconds Max |
|  | @ +60 °C | Clear, No sediment | Sediment not to exceed 0.05% v/v |
| Compatibility | @ -40 °C | Clear, No stratification | No stratification |
|  | @ +60 °C | Clear, No sediment | Sediment not to exceed 0.05% v/v |
| Colour, visual |  | Pale Straw | Water white to amber |
| Water Content, % |  | 0.11 | <0.15 |
| Density @ 20 °C, g/ml |  | 1.065 | Not required |