PRODUCT DESCRIPTION AND PERFORMANCE SPECIFICATION

OIL UK LHM PLUS is a high performance LHM Fluid which fully meet the requirements of the latest issue of the ISO 7308 Specification.

| TYPICAL PHYSICAL CHARACTERISTICS |  |
| --- | --- |

| Test Required |  | Typical Results | Specification |
| --- | --- | --- | --- |
| Equilibrium Reflux Boiling Point, °C | 253 | 270 °C Min |
| Kinematic Viscosity | @ +100 °C, cSt | 6.30 | 6.0 to 6.8 cSt |
|  | @ +40 °C, cSt | 18.48 | 18.0 to 20.0 cSt |
|  | @ -40 °C, cSt | 1068 | 1000 to 1200 cSt |
| Viscosity Index |  | 341 | 310 Min |
| Flash Point, PM Closed Cup, °C |  | 110 °C Min |
| Pour Point, °C |  |  | -50 °C Max |
| Water Content, ppm |  | 35 | 50 ppm Max |
| Neutralisation Index, mg KOH/g | 0.092 | 0.1 Max |  |
| Fluidity & Appearance | @ -40 °C | Pass, 3 second | No freezing, Bubble time 10 sec. Max |
|  | @ -50 °C | Pass, 9 seconds | No freezing, Bubble time 35 sec. Max |
| Hydroscopicity |  | -0.031 | 0.1 Max |
| Foam Volume | @ 24 °C, ml | 80 | 100 Max |
|  | @ 93 °C, ml | 40 | 200 Max |
|  | Cooled to 24 °C | 80 | 100 Max |
|  | 2 Min @ 24 °C | 0 | Nil |
|  | 2 Min @ 93 °C | 0 | Nil |
| Compatibility | @ -40 °C | Pass | Clear - no stratification or sedimentation |
|  | @ +60 °C | Pass | Clear - no stratification or sedimentation |
| Shear stability (175Bar, 250 cycles), ΔcSt | -0.02 | 0.5 cSt Decrease Max |
| Anti-wear stability (4 ball), mm wear | 0.529 | 1 mm Max |
| Colour, visual |  | Green | Green |