PRODUCT DESCRIPTION

OIL UK NO-RUST WLT is a solvent deposited, firm wax film corrosion preventive. This product gives long term protection on ferrous and aluminium alloy components and is particularly suited to outdoor storage conditions and protection of machinery, bearings, parts and components etc. during sea voyages.

RUST PREVENTIVE PERIOD

- Indoors:		Minimum 4 Years

- Outdoors, Covered:	Minimum 3 Years

- Outdoors:		Minimum 1 Year

Figures are dependent upon correct application procedures being followed. It is not necessary to remove the coating prior to installing bearings just re-grease.

PERFORMANCE BENEFITS

- Excellent resistance to water

- Wax film giving chemical & physical protection

- Long term protection

- Good coverage

- Universal application

- Thixotropic

- Cost Effective

METHOD OF APPLICATION

Dip Tank: Ensure ambient temperature is above 5°C or product will be too viscous for this type of application. Submerge components in fluid for 20 seconds and then raise and allow to drain. Place in drying area for up to 1 hour depending upon surrounding temperature and air flow.

Brush or Spray: Liberally apply to components and allow to dry.

COVERING CAPACITY & REMOVAL

Covering Capacity: 	20-30 sq.metres/litre. Depending on application temperature

Removal:	Can be removed with hydrocarbon solvents or hot alkaline cleaners

| TYPICAL PHYSICAL CHARACTERISTICS |
| --- |
| Appearance | Opaque Brown Fluid |
| Dried Film | Firm Wax |
| Film Thickness | 8 Microns Dipped @ 20°C |
| Hot Salt Spray | ASTMB117 250 hours |
| Humidity - Hours | BS3900F4 750-1000 |
| Flash Point | 40°C |