PRODUCT DESCRIPTION

OIL UK NO-RUST A is a solvent deposited waxy film corrosion preventative suitable for long term storage indoors and outdoors. Conforms to BS TP IC (BS1133 Section 6).

OIL UK No-Rust A is designed to give a thick flexible waxy protection coating, suitable for the protection of ferrous and non-ferrous components and machinery for in excess of 3 years indoors uncovered and 2 years outdoor covered storage.

The product contains a volatile hydrocarbon solvent for ease of application and dries in approximately one hour to a thin flexible film.

OIL UK No-Rust A exhibits excellent humidity cabinet results and salt spray results (e.g. on phosphated components gives in excess of 2,000 hours).

RUST PREVENTIVE PERIOD

- INDOOR: At least 36 months

- OUTDOOR: 24 months (under cover).

METHOD OF APPLICATION

- For best results components should be dipped in OIL-UK No-Rust A

- . OIL-UK No-Rust A can also be applied by brush or spray.

CLEANING

Oil UK No-Rust A can easily be removed by traditional degreasing with solvent or alkaline cleaners.

TYPICAL PHYSICAL DATA

| TEST | DATA |
| --- | --- |
| Appearance - Fluid | Opaque brown fluid |
| Appearance – Dried Film | Flexible waxy film |
| Flash Point °C | 40 |
| Specific Gravity | 0.87 |

.