PRODUCT DESCRIPTION

OIL UK NO-RUST RP-S is a solvent deposited, water displacing, light, oil/grease film corrosion preventive. This product gives medium to short-term protection on ferrous or aluminium alloy components, sheets and tubes and is particularly suited for inter-shop protection after machining or washing operations and any indoor short term storage. This very light oil almost dry film gives excellent rust inhibition and water protection.  Ideal for the storage of components and machinery.  Easily washes off with hot soapy water if required. Based on low odour solvents to improve operator acceptability and reduce environmental impact.

RUST PREVENTIVE PERIOD

- Indoors:		Minimum 12 months

- Outdoors, Covered:	Minimum 3 months

- Outdoors:		Not recommended

Figures are dependent upon correct application procedures being followed.

PERFORMANCE BENEFITS

- Excellent de-watering properties

- Light film - no need to clean before assembly

- Contains finger print suppressant

- Good coverage

- Excellent demulsification

- Low odour

- Drying Time 30 minutes

- Non Volatiles 16%

- Flash Point 40°C

- Cost Effective

METHOD OF APPLICATION

Dip Tank: Using a wire basket, submerge components for 30 seconds minimum. Lift from fluid; allow draining and stack to dry. Drain tank of excess water periodically.

Brush or Spray: Liberally apply to components and allow drying.

COVERING CAPACITY & REMOVAL

Covering Capacity: 	70 sq. metres/litre @ 2.2 microns (dipped)

Removal:	If required, can be removed with hydrocarbon solvents or hot alkaline cleaners

| TYPICAL PHYSICAL CHARACTERISTICS |
| --- |
| Appearance | Clear Red/Brown Fluid |
| Dried Film | Light Grease/Oil |
| Film Thickness | 2.2 Microns Dipped @ 20°C |
| Hot Salt Spray | ASTMB117 Min. 30 hours |
| Dewatering Test BS1133 62B | No Corrosion |
| Flash Point | 40°C |