PRODUCT DESCRIPTION

OIL-UK NO-RUST PLUS is a rapid water displacing fluid, which on evaporation of the solvent deposits an oil protective film. It may therefore be applied to wet or dry parts. When wet parts are dipped into a tank of OIL-UK No-Rust Plus the water is displaced rapidly and efficiently without the product itself becoming contaminated with water. It therefore has a long life, which can be extended by regular draining off of precipitated water. After evaporation of the solvent a thin oily film is deposited onto the metal surface to give long term indoor protection, and medium term outdoor protection.

TYPICAL APPLICATIONS

- Inter process protection following machining or grinding with water-based fluids

- Following water based cleaning operations

- Following water based deburring operations

- Storage or shipment where a thin film is desirable.

RUST PREVENTIVE PERIOD

- INDOOR: At least 24 months

- OUTDOOR: 3 months (under cover).

METHOD OF APPLICATION

- For best results components should be dipped in OIL-UK No-Rust Plus and for this purpose a tank fitted with a sloping bottom and drain plug is desirable.

- Water should be drawn off frequently and care should be taken to ensure that dipped articles do not come into contact with the accumulated water.

- Hollow articles or those with water traps should be allowed to drain completely so that small pockets of water are not held in contact with the metal surface resulting in rust spotting. OIL-UK No-Rust Plus can also be applied by brush or spray.

CLEANING

The removal of the protective film is not normally necessary prior to assembly of components or further machining. However, it can easily be removed by traditional degreasing with solvent or alkaline cleaners.

TYPICAL PHYSICAL DATA

| TEST | DATA |
| --- | --- |
| Viscosity @ 40°C cSt | 4.0 |
| Flash Point °C | 80 |
| Humidity Cabinet ASTM D2247-11 60 Days | Pass |
| Salt Fog ASTM B117 Resistance | 24 hrs |

.