PRODUCT DESCRIPTION

OIL UK NO-RUST DF is a fast drying rust prevention fluid, which on evaporation of the solvent deposits a thin dry to touch oil protective film.  After evaporation of the solvent a thin oily film of around 1 micron is deposited onto the metal surface to give medium term indoor protection, and short term covered outdoor protection.

1 litre of Oil UK No-Rust DF will provide coverage of an area of approximately 50m2. This product is suitable for both ferrous and non-ferrous metals.

RUST PREVENTIVE PERIOD

- INDOOR: 12 months

- OUTDOOR: 3 months (under cover).

| PERFORMANCE BENEFITS |
| --- |
| Excellent corrosion prevention | Longer term storage |
| Fast evaporating | Drier quicker for packing |
| Cost effective | Very economical in-use |
| Dry to touch | Suitable for handling |

METHOD OF APPLICATION

- For best results components should be dipped in OIL-UK NO-RUST DF and for this purpose a tank fitted with a sloping bottom and drain plug is desirable.

- OIL-UK NO-RUST DF can also be applied by brush or spray.

| TYPICAL PHYSICAL CHARACTERISTICS |
| --- |
| Appearance | Pale fluid |
| Specific Gravity | ~0.83 @ 20oC |
| Foaming Tendency | Low |
| Viscosity at 40oC | 1.8 cSt |
| Humidity cabinet protection | 60+ |