DESCRIPTION

OIL UK SOLCUT 500 XF is a medium oil content product containing chlorine free lubricity additives which give excellent cutting performance and surface finish on tough ferrous and non-ferrous alloys, including aerospace aluminium grades and titanium.

SOLCUT 500 XF is extremely low foaming and performs well in through spindle and high coolant volume delivery applications.

SOLCUT 500 XF is an extremely robust coolant and gives extended service life in the most difficult conditions.

FEATURES AND BENEFITS

- Enhanced Health and Safety - Secondary amine free, Boron free, Formaldehyde Biocide free

- Loaded with lubricity components for enhanced tool life and excellent surface finish

- Suitable for both moderate and highly arduous applications

- Low foaming tendency in high pressure systems and suitable for both hard and soft water qualities

- Multi-metal compatible. Suitable for both ferrous and non-ferrous materials

- Provides long, low odour coolant life and excellent machine tool cleanliness

- Excellent cost saving potential through enhanced tool life

- Extra high levels of corrosion protection

MATERIAL SUITABILITY AND RECOMMENDED CONCENTRATIONS

| Material Type | Performance Rating | Recommended Concentration General Purpose | Recommended Concentration Heavy Duty |
| --- | --- | --- | --- |
| Aluminium & Titanium Alloys | XXXXX | 5-7% | 8-10% |
| High Alloy/Stainless Steels | XXXXX | 5-7% | 8-10% |
| Low to medium tensile steels | XXXXX | 5-7% | 8-10% |
| Copper/Brass | XXXXX | 5-7% | 8-10% |
| Cast Iron | XX | 4-6% | 5-8% |
| Machining Operations |  |  |
| Turning, Milling Drilling | 4-6% | 7-8% |
| Tapping & Threading | 5-7% | 9-12% |
| Reaming and deep hole drilling | 7-9% | 10-12% |

TYPICAL PHYSICAL PROPERTIES

| Appearance - Emulsion | Semi Translucent |
| --- | --- |
| pH at 5% in distilled water | 9.7 |
| IP 287 Corrosion break point | 2.0 |
| Refractometer correction factor | 1.4 |