DESCRIPTION

OIL UK SOLCUT 400 XF is a high performance Semi Synthetic, formaldehyde release biocide free, watermix fluid designed for tough machining operations in situations where foaming may be a problem.

OIL UK SOLCUT 400 XF is a medium oil content product containing chlorine free synthetic ester extreme pressure and lubricity additives which give excellent cutting performance and surface finish.

SOLCUT 400 XF is extremely low foaming and works well in soft water areas. It is well suited for use on a variety of steel alloys including stainless steel and titanium and can be used for the machining of non-ferrous alloys.

SOLCUT 400 XF is an extremely robust coolant and gives extended service life in the most difficult conditions.

FEATURES AND BENEFITS

- Enhanced Health and Safety - Formaldehyde free

- Loaded with lubricity components for enhanced tool life and excellent surface finish

- Suitable for both moderate and highly arduous applications

- Low foaming tendency in high pressure systems and suitable for both hard and soft water qualities

- Multi-metal compatible. Suitable for both ferrous and non-ferrous materials

- Provides long, low odour coolant life and excellent machine tool cleanliness

- Excellent cost saving potential through enhanced tool life

- Extra high levels of corrosion protection

MATERIAL SUITABILITY AND RECOMMENDED CONCENTRATIONS

| Material Type | Performance Rating | Recommended Concentration General Purpose | Recommended Concentration Heavy Duty |
| --- | --- | --- | --- |
| Aluminium & Titanium Alloys | XXXXX | 5-7% | 8-10% |
| High Alloy/Stainless Steels | XXXXX | 5-7% | 8-10% |
| Low to medium tensile steels | XXXXX | 5-7% | 8-10% |
| Copper/Brass | XXXXX | 5-7% | 8-10% |
| Cast Iron | XX | 4-6% | 5-8% |
| Machining Operations |  |  |
| Turning, Milling Drilling | 4-6% | 7-8% |
| Tapping & Threading | 5-7% | 9-12% |
| Creep feed grinding | 7% | 8% |
| Surface, cylindrical & centreless grinding operations | 3-4% |

TYPICAL PHYSICAL PROPERTIES

| Appearance - Emulsion | Semi Translucent |
| --- | --- |
| pH at 5% in distilled water | 9.3 |
| IP 287 Corrosion break point | 2.0 |
| Refractometer correction factor | 1.0 |