DESCRIPTION

OIL UK SOLCUT 300 EP-XF is a high performance Semi Synthetic, formaldehyde release biocide free, watermix fluid designed for arduous machining operations. OIL UK SOLCUT 300 EP-XF is a medium oil content product containing selected extreme pressure and lubricity additives to provide superb machining performance in tough machining operations.

SOLCUT 300 EP-XF is extremely low foaming and works well in both hard and soft waters. It is well suited for use on a variety of steel alloys and can also be used for the machining of non-ferrous alloys.

SOLCUT 300 EP-XF is an extremely robust coolant and gives extended service life in the most difficult conditions.

FEATURES AND BENEFITS

- Enhanced Health and Safety - Formaldehyde free

- Loaded with lubricity components for enhanced tool life and excellent surface finish

- Suitable for both moderate and highly arduous applications

- Low foaming tendency in high pressure systems and suitable for both hard and soft water qualities

- Multi-metal compatible. Suitable for both ferrous and non-ferrous materials

- Provides long, low odour coolant life and excellent machine tool cleanliness

- Excellent cost saving potential through enhanced tool life

- Extra high levels of corrosion protection

MATERIAL SUITABILITY AND RECOMMENDED CONCENTRATIONS

| Material Type | Performance Rating | Recommended Concentration General Purpose | Recommended Concentration Heavy Duty |
| --- | --- | --- | --- |
| Aluminium Alloys | XXXX | 5-7% | 8-10% |
| High Alloy/Stainless Steels | XXXXX | 5-7% | 8-10% |
| Low to medium tensile steels | XXXXX | 5-7% | 8-10% |
| Copper/Brass | XXXX | 5-7% | 8-10% |
| Cast Iron | XX | 4-6% | 5-8% |
| Machining Operations |  |  |
| Turning, Milling Drilling | 4-6% | 7-8% |
| Tapping & Threading | 5-7% | 9-12% |
| Reaming & deep hole drilling | 7-10% | 12% |
| Surface & cylindrical grinding operations | 3-4% |

TYPICAL PHYSICAL PROPERTIES

| Appearance - Emulsion | Semi Translucent |
| --- | --- |
| pH at 5% in distilled water | 9.3 |
| IP 287 Corrosion break point | 2.5 |
| Refractometer correction factor | 1.1 |