DESCRIPTION

OIL UK SOL-GRIND S-XF is a fully synthetic, formaldehyde release biocide free, watermix grinding fluid suitable for surface and cylindrical grinding. This high performance universal grinding fluid can be used to grind all ferrous and non-ferrous materials including yellow metals.

OIL UK SOL-GRIND S-XF gives superb low foam performance and has an extremely long service life. This product contains a polymer based lubricity additive to give enhanced grinding performance, and does not give sticky residues around the machine tool during use.

APPLICATIONS

Surface & cylindrical grinding.

Recommended dilution: 3% to 4%

MATERIALS SUITABILITY

| Ferrous alloys Aluminium alloys Yellow metals Nickel Alloys and Titanium |  |
| --- | --- |
| TYPICAL PHYSICAL PROPERTIES |

| OIL UK SOL-GRIND S-XF |  |
| --- | --- |
| Appearance - Emulsion | Green, translucent |
| Foaming Tendency | Very Low |
| pH @ 5% | 9.5 |
| Refractometer Factor | 3.3 |
| IP 287 corrosion break point | 2.0 |