PRODUCT DESCRIPTION

OIL-UK TURBINE EP is a range of superior quality heavy duty Turbine Oil manufactured from the highest quality solvent refined base oils combined with special performance additives. These state of the art additive systems offer outstanding protection against oxidation and long-term corrosion protection. Special demulsibility additives provide excellent water separation properties to protect against water ingress.

APPLICATIONS

OIL-UK TURBINE EP oils provides excellent lubrication and cooling of turbine and generator bearings, couplings and reduction gears in the most demanding turbine systems including those operating in highly arduous conditions, where high anti-wear properties are essential This product can also be used for lubricating air compressors and as an extreme duty hydraulic fluid and circulatory system oil.

FEATURES AND BENEFITS

- Excellent extreme pressure performance

- Superior oxidation stability

- Long term corrosion protection

- Superb water separation

- High viscosity Index

- Outstanding anti-foam properties

- Compatible with all commonly used seal materials

PERFORMANCE SPECIFICATIONS

ASTM D-4304 TYPE I & TYPE III, ALSTOM HTGD 90117, BRITISH STANDARD BS 489, DENISON HF-1, CINCINNATI MILACRON P-38 (ISO 32), P-54 (ISO 68),P-55 (ISO 46) & P-57 (ISO 150), DIN 51524 PART 1, 51515 PART 1: L-TD & PART 2: L-TG GENERAL ELECTRIC GEK-32568F, ISO 8068 L-TGB & L-TGSB, 6743-5 L-TSA & L-TGA, 11158 HH & HL, US STEEL 120 & 126, MILITARY MIL-L-17672 C, AFNOR E-48600 HL, SIEMENS AG TLV 9013 04 (STANDARD THERMAL STABILITY) & TLV 9013 05 (HIGH THERMAL STABILITY), BROWN BOVERI HTGD 90117

TYPICAL PHYSICAL DATA

| PROPERTY | ISO 32 | ISO 46 | ISO 68 | ISO 100 | ISO 150 | ISO 220 | ISO 320 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ISO Viscosity Grade | 32 | 46 | 68 | 100 | 150 | 220 | 320 |
| Specific Gravity @ 15.60°C | 0.873 | 0.878 | 0.884 | 0.889 | 0.890 | 0.893 | 0.895 |
| Kinematic Viscosity @ 40°C, cSt | 32 | 46 | 68 | 100 | 150 | 220 | 320 |
| Flash Point °C, COC | 216 | 220 | 235 | 225 | 230 | 235 | 237 |
| Viscosity Index | 102 | 102 | 104 | 100 | 100 | 101 | 99 |