PRODUCT DESCRIPTION

Oil UK Flushing Additive Concentrate is a blend of non-corrosive high flash point materials, completely soluble in mineral oil, which has a high solvent action on gums and varnishes.

All mineral oils are susceptible to oxidation even though the rate of oxidation is considerably retarded in those higher grade products (such as Oil UK Therm Oils) based on specially refined oils and incorporating the correct anti-oxidants. Mineral oil oxidation results in the formation of organic acids, alcohols, ketones and aldehydes most of which are soluble in the oil and increase its acidity and viscosity. In time, however, some of the above compounds form insoluble gums on heater coils, and sludge and varnish causing reduced performance in heat transfer systems.

Oil UK Flushing Additive Concentrate removes such oxidation products and quickly restores cleanliness, thermal stability and trouble-free operation

FEATURES

- High flash point (110ºC) compared with many solvent cleaners

- Exceptional solvent power for gums and varnishes

- Dissolves small amounts (less than 1%) of water

- Ease of application – No loss of production time

- Restores full system efficiency

METHOD OF APPLICATION

Best results are obtained by adding Oil UK Flushing Additive Concentrate to the system in the proportion of 5% of the system heat transfer fluid volume content, i.e. 50 litres of additive for every 1,000 litres of heat transfer fluid. The system should then be operated for 100-150 hours before draining and filling with new oil.

Flushing Additive Concentrate does not neutralize the acidic products of mineral oil oxidation. Therefore draining after the specified period is essential. Flushing Additive Concentrate is also highly effective in removing gear oil oxidation residues, rolling oil residues, while in oil-filled heat transfer systems use of the product improves efficiency by removing gums from heater coils. After the use of Flushing Additive Concentrate all filters should be thoroughly cleaned before the introduction of new oil.