PRODUCT DESCRIPTION

OIL UK ANGLO-MAX SUPER XDM-E9 15W-40 is the very latest, new generation Super High Performance heavy duty diesel engine oil formulated to meet the latest Euro 5 & 6 low emissions requirements. This advanced lubricant utilises the latest mid SAPS additive technology which helps protect sensitive after-treatment systems found in many modern heavy duty vehicles. It is a new generation Group II based commercial vehicle engine oil and is compatible with the latest emission compliant engines from manufacturers such as Volvo and Renault.

APPLICATIONS

ANGLO-MAX SUPER XDM-E9 15W-40 has a wide range of applications including original equipment manufacturers (OEMs) such as Volvo, Scania, Renault, Mercedes, DAF and MAN. It is also an ideal choice for many buses, tractors and off-highway applications particularly where the latest low emission engines are used.

Typical oil change intervals (Always adhere to vehicle manufacturer’s recommendation)

| CONDITIONS: | SEVERE | DIFFICULT | MODERATE | GOOD | VERY GOOD |
| --- | --- | --- | --- | --- | --- |
| KMS: | 25,000 | 50,000 | 70,000 | 85,000 | 100,000 |

FEATURES AND BENEFITS

- Outstanding Protection – ANGLO-MAX SUPER XDM E9 15w-40 features an exclusive additive system to ensure maximum soot handling, excellent wear protection and extra-long oil life.

- Environmental Benefits – Reduced C02 and pollutant emissions

- High Performance – ANGLO-MAX SUPER XDM E9 15w-40 adapts and protects under the full range of pressures and temperatures found in modern engines, including those operating constantly in high ambient temperatures.

- Improved Engine Cleanliness – The latest generation additive system in ANGLO-MAX SUPER XDM E9 10w-30 delivers improved engine cleanliness and protection against piston deposits.

- Manufacturers Standards - ANGLO-MAX SUPER XDM E9 15w-40 satisfies and exceeds the most demanding performance standards of major international engine manufacturers and oil and motor vehicle industry specifications.

PERFORMANCE SPECIFICATIONS

ACEA E9, API CK-4, CJ-4, SM/CF,

CUMMINS CES 20081, MB 228.31, MAN M3575 M3275, MTU TYPE 2.1, RENAULT RVI RLD-3, VOLVO VDS-4, CATERPILLAR ECF-3, MACK EO-O PREM PLUS, Global DH-1, JASO DH-1,DH-2

TYPICAL PHYSICAL CHARACTERISTICS

| Test | Units | Test Method | Typical Properties |
| --- | --- | --- | --- |
| Appearance |  | Visual | Clear and Bright |
| Specific Gravity @ 15.5°C |  |  | 0.878 |
| Kinematic Viscosity @ 100°C | cSt | ASTM D445 | 14.93 |
| Kinematic Viscosity @ 40°C | cSt | ASTM D445 | 113.70 |
| Viscosity Index |  | ASTM D2270 | 136 |
| Flash Point (Open) | °C | ASTM D92 | 230 |
| Pour Point | °C | ASTM D97 | -30 |
| Total Base Number | mg KOH/g | ASTM D2986 | 9.2 |
| Sulphated Ash | (% weight) |  | 1.00 max. |