DESCRIPTION

OIL UK ANGLO-MAX SUPER LS-GM 5W-30 is a new generation fully synthetic multigrade engine oil formulated from premium hydrocracked synthetic base stocks, the very latest detergent-dispersant additive package and shear stable polymers.

The reduced levels of SAPS (sulphated ash, phosphorus and sulphur) in SUPER LS-GM 5W-30 ensures compatibility with after treatment systems, such as particulate filters and catalytic converters, and its frictional characteristics promote a reduction in fuel consumption.

APPLICATIONS

OIL UK ANGLO-MAX SUPER LS-GM 5W-30 is recommended for use in a wide variety of passenger cars and vans fitted with petrol and diesel engines. Manufacturers include Chrysler, Citroen, Daewoo, Daihatsu, Honda, Hyundai, Isuzu, Land Rover, Lexus, Mazda, Mercedes Benz, Nissan, Peugeot, Renault, Saab, Subaru, Suzuki, Toyota and Vauxhall.

Typical oil change intervals (Always adhere to vehicle manufacturer’s recommendation)

| CONDITIONS: | SEVERE | DIFFICULT | MODERATE | GOOD |
| --- | --- | --- | --- | --- |
| KMS: | 10,000 | 20,000 | 30,000 | 40,000 |

FEATURES AND BENEFITS

- After treatment system compatible

- Extended drain intervals

- Promotes reduced fuel consumption

- Ensures maximum engine protection

- Excellent high and low temperature stability

PERFORMANCE SPECIFICATIONS

API ACEA General Motors Mercedes Benz PSA SN/CF C2, C3 Dexos 2 MB 229.52/229.51/229.31 PSA B71 2290

| TYPICAL PHYSICAL DATA |
| --- |
| PROPERTY | TYPICAL DATA |
| Kinematic Viscosity @100°C (cSt) | 12.30 |
| Kinematic Viscosity @ 40°C (cSt) | 73.1 |
| Viscosity Index | 167 |
| Density @15°C | 0.852 |
| Flash Point, COC (°C) | 230 |
| TBN (mgKOH/g) | 7.5 |
| Cold Cranking Viscosity @ -30°C (Cp) | 5650 |