OIL UK GEARLUBE SUPER SS 75W-80 HIGH PERFORMANCE SEMI-SYNTHETIC AUTOMOTIVE GEAR OIL

PRODUCT DESCRIPTION

OIL UK GEARLUBE SUPER SS 75W-80 is a premium semi-synthetic manual transmission fluid recommended for use in a wide range of passenger cars and vans on the road today.

GEARLUBE  75W-80 exceeds the performance levels of more conventional API GL-4/GL-5 lubricants in terms of synchroniser performance, thermal and oxidative stability, shift quality and fuel efficiency. In addition, this product allows considerable rationalisation for out of warranty service fill by being able to replace OEM genuine oils. Performance Specification: API: GL-5

PRODUCT APPLICATIONS

OIL UK GEARLUBE SUPER SS 75W-80 is recommended for use in a wide variety of manual transmissions in passenger cars and vans that are out of vehicle warranty where an SAE 75W-80 viscosity grade is required.

OIL UK GEARLUBE SUPER SS 75W-80 is recommended where the specification MTF-94 is called for.

- BMW

- CITROEN

- ALFA ROMEO

- VOLKSWAGEN

- MINI

- PEUGEOT

- FIAT

- SEAT

- MERCEDES

- RENAULT

- VOLVO

- SKODA

- SMART

- DACIA

- HONDA

VAUXHALL

FEATURES AND BENEFITS

- Improved synchromesh performance

- Improved shift quality

- Load carrying durability

- Maximum component protection

- High levels of oxidation resistance

- Outstanding thermal stability

| TYPICAL PHYSICAL DATA |
| --- |
| PROPERTY | UNIT | TYPICAL DATA |
| Specific Gravity @ 15.5°C | g/ml | 0.875 |
| Kinematic Viscosity @ 100°C | cSt | 9.1 |
| Kinematic Viscosity @ 40°C | cSt | 58 |
| Viscosity Index |  | 136 |
| Flash Point (COC) | °C | 220 |
| Pour Point | °C | -45 |