OIL UK GEARLUBE SUPER SS 75W-90 HIGH PERFORMANCE SEMI-SYNTHETIC AUTOMOTIVE GEAR OIL

PRODUCT DESCRIPTION

OIL UK GEARLUBE SUPER SS 75W-90 is a semi synthetic gear oil manufactured from very high quality synthetic and premium mineral base stocks, highly effective extreme pressure and anti-wear additives and shear stable viscosity modifiers.

Gearlube SS 75W-90 offers unsurpassed load carrying capacity, which is essential for shock load, high torque and high speed service operation. The high thermal stability of the product’s components allows extended oil drain intervals to be realised and the levels of protection provided ensure maximum component durability.

Performance Specification: API: GL-5

PRODUCT APPLICATIONS

OIL UK GEARLUBE SUPER SS 75W-90 is recommended for a variety of highly stressed manual gearboxes, heavily loaded axle drives, transfer boxes and other transmission equipment found in many passenger cars, light and heavy duty commercial vehicles and off-highway applications.

FEATURES AND BENEFITS

- Semi-synthetic

- long oil drain formulation

- Excellent low temperature fluidity

- Maximum component protection

- High levels of oxidation resistance

- Outstanding thermal stability

| TYPICAL PHYSICAL DATA |
| --- |
| PROPERTY | UNIT | TEST METHOD | TYPICAL DATA |
| Specific Gravity @ 15.5°C | g/ml | ASTM D4052 | 0.865 |
| Kinematic Viscosity @ 100°C | cSt | ASTM D445 | 14.5 |
| Kinematic Viscosity @ 40°C | cSt | ASTM D445 | 94 |
| Viscosity Index |  | ASTM D2270 | 160 |
| Flash Point (COC) | °C | ASTM D92 | 220 |
| Brookfield Viscosity @ -40°C | cP |  | 125,000 |